Rare earth acylpyrazolonates - synthesis, structure, luminescent properties and applications

Yuriy A. Belousov1,2,3*, Andrei A. Drozdov1, Daniil D. Shikin1,2, Alessia Tombesi4, Riccardo Pettinari4, Fabio Marchetti5 and Claudio Pettinari4*

- Chemistry Department, Moscow State University, Leninskie Gory, Moscow, 119991, Russia;

- P. N. Lebedev Physical Institute of the Russian Academy of Sciences, 53 Leninskiy 1. Prospect, Moscow, 119991, Russia

- Faculty of Chemistry, National Research University Higher School of Economics, 20 Miasnitskaya Str., 101000 Moscow, Russia

- ChIP Research Center, School of Pharmacy, University of Camerino, via Madonna delle Carceri, 62032 Camerino MC, Italy – Istituto di Chimica dei Composti Organometallici (ICCOM-CNR) Florence

- ChIP Research Center, School of Science and Technology, University of Camerino, via Madonna delle Carceri, 62032 Camerino MC, Italy.

Abstract

Acylpyrazolonate derivatives of rare earth elements (REE), being a non-mainstream class of b-diketonates, have continued to attract chemists and materials scientists for more than half a century. The electronic structure features of these ligands make them effective sensitizers of the luminescence of various lanthanides, emitting in the visible and IR regions. Exhibiting all the typical structural types of b-diketonates, acylpyrazolonates can form heterometallic complexes with d-elements due to the presence of additional donor atoms. The review covers more than half a century of the history of these compounds and provides a perspective on the development of this class of compounds and their transformation into materials of the 21st century.

Introduction

At least two distinct reasons have rendered the alliance of acylpyrazolones and Ln3+ ions a significant chapter in the coordination chemistry of f-elements. The first reason is the use of acylpyrazolones for the extraction separation of Ln3+ ions as well as the separation of 4f- and 5f-elements. This crucial chapter was initiated by the Danish chemist Bror Skytte Jensen in 1959 [1,2], who marked the beginning of an exponential surge in interest towards f-element chemistry, which evolved over several decades [3–7] and continues to be explored to this day [8].

The discovery of the antenna sensitization effect by Weissman in 1942 [9] laid the groundwork for the development of the entire coordination chemistry of lanthanides [10,11], as it paved the way for the creation of molecular luminescent complexes of these elements. Antenna sensitization is critically important because it addresses the primary challenge of lanthanide luminescent materials by replacing the inefficient direct photoexcitation of Ln3+ with excitation via an organic ligand – the antenna [10–13]. Among the numerous ligands used in luminescent lanthanide complexes, acylpyrazolonates have occupied a special niche since the 1970s [14,15], as they retain the fundamental properties of β-diketonates while providing higher triplet level energy, thereby enabling more efficient sensitization of Tb3+ and Dy3+ emission.

In this review, we will discuss the structures, synthesis methods, luminescent properties, and potential applications of lanthanide complexes with acylpyrazolonates. The focus will primarily be on articles that contain X-ray structural and luminescent studies data. With the exception of the only described Ce(IV) complex[16], only Ln3+ derivatives will be considered.

Ligands, Tautomerism, and Synthesis

Acylpyrazolones represent a heterocyclic class of β-diketones, characterized by the presence of a chelating group within the pyrazole ring. Although they were first synthesized in the 19th century, it was not until 1959 that Bror Skytte Jensen, in his quest for new chelating agents, discovered a convenient method for the synthesis of 3-methyl-1-phenyl-4-acylpyrazol-5-one [1] which involves the following steps. Initially, 3-methyl-1-phenylpyrazol-5-one is obtained via condensation of phenylhydrazine with ethyl acetoacetate or its protected derivatives [17–21]. This reaction is typically conducted in glacial acetic acid [22–24], though ethanol [25–27] or other solvents such as methanol [28], isopropanol [27], chloroform [20], THF, and subsequently toluene [29], xylene [30] or glycerol [31] under acidic catalysis conditions can be employed. Following this, acylation of the corresponding pyrazolone with an acyl chloride is carried out under reflux in dioxane in the presence of calcium [1] or barium [30,32] hydroxide or calcium oxide [33]. Finally, the reaction mixture is treated with hydrochloric acid solution to break down the calcium complex [1,17,18]. This method yields a high output and offers significant versatility: to obtain an acylpyrazolone with different substituents, one simply needs to use appropriately substituted hydrazine, acetoacetate, and acyl chloride.

The numbering in the ring of acylpyrazol-5-one starts from the substituted atom towards the second heteroatom, ending at the keto group. Previously, we proposed [17] a simple scheme for designating 4-acylpyrazol-5-ones: HQR1,R2,R3, where H represents a mobile proton that can be released during [QR1,R2,R3]- anion formation. Since the majority of HQ proligands are compounds for which R1 = Ph and R2 = Me, an abbreviated notation is used in such cases: HQR3. For bis(acylpyrazolones), where two 4-acylpyrazol-5-one fragments are separated by a bridge -R-, the abbreviation is written as H2QRQ, and if R = (CH2)n, the formula appears as H2QnQ. The only described tris(acylpyrazolone) to date reported will be abbreviated similarly as H3QRQQ (R = 1,3,5-C6H3). Lanthanide complexes containing acylpyrazolonate ligands are listed in Table 1 together with energies of the singlet (S) and triplet (T) levels of the ligands and the extinction coefficients (e) reported when they were determined in the original publications.

Table 1. S, T and e of acylpyrazolonate lanthanide complexes.

| Proligand employed in the synthesis | Ln3+ ions for which complexes have been reported and relative reference | S, cm-1 | T, cm-1 a | ε, M-1cm-1 (λmax, nm) Q- anionb |
| --- | --- | --- | --- | --- |
| Proligands with R1=Ph and R2=Me |  |  |  |  |
| HQH | Nd, Sm, Eu, Tb[34]; Nd, Sm, Eu, Gd, Tb, Dy, Tb [35]; Nd, Sm, Eu, Tb [36]; Tb [37] | 24150[34] | 20700 [34] | n/a (300 nm) [36] |
| HQMe | Dy[38]; Tb, Gd [39]; Tb [40] |  | 23000 [38] 23900 (20580)a [39] | (335 nm [38]) 6.89*104 (262 nm) [39] |
| HQEt | Tb, Gd [39]; Tb [40] |  | 24300 (20370)a [39] | 6.94*104 (262 nm) [39] |
| HQOEt | Tb [40] |  |  |  |
| HQnPr | Tb [40] |  |  |  |
| HQNMe2 | Tb [40] |  |  |  |
| HQiPr | Tb, Gd [39]; Tb[41]; Y, Nd, Gd, Tm, Er, Tm, Lu; Sm, Gd [42]; Yb, Gd [43]; Dy [44]; Eu [45]; Y, Nd, Gd, Tb, Er, Tm, Lu [46]; Eu, Gd [47]; Tb [48]; Lu [49]; Gd, Dy [50]; Er [51]; Gd [52]; Nd [53]; Tb [54]; Tb [40]; Tb [55]; Tb [56]; Tb [57]; Tb [58]; Gd [59]; Tb [60]; Tb [61] | 32785 [47] | 23900 (19340)a [39] 24500 (23000)a [41] 21460 [42] 24500(21740)a [43] 25000 (23500)a [47] 25000(21460)a [50] | 7.14*104 (262 nm) [39] 3.5*104 (265 nm) [47] 3.1*104 (266 nm) [58] |
| HQtBu | Tb, Gd [39]; Pr, Nd, Gd, Tb, Tm, Lu [62]; Tb [63]; Tb, Gd [64] |  | 22300 (18180)a [39] 22500(21000)a [64] | 6.84*104 (263 nm) [39] |
| HQCH2tBu | Tb, Gd[65]; Sm, Gd, Tb [66]; La, Sm, Gd [67]; Tb, Dy [68] | 30730[65] 27624[67] | 21505 [65] 23500(23041)a [67] |  |
| HQCH2Cl | Eu [69] |  |  | 5.5*104 (256 nm) [69] |
| HQCHEt2 | Tb, Gd [70]; Tb [71]; Tb [56]; | 28736 [70] | 23585 [70] |  |
| HQCP | Tb [72]; Eu, Tb [73]; Eu, Tb, Gd [74] |  | 23000 (20800)a [74] |  |
| HQCY | Eu, Gd [75]; Dy, DyxGd1-x, Gd [76]; Sm, Pr, Nd [77], Sc, La, Gd, Lu [78]; Tb, Eu [79], Sm, Eu, Gd, Tb, Dy [80] | 29400 [75] 28500 [77] | 23640 (exp) 24040 (calc) [75] 23600 [78] | 3.2-5.5*104 (268 nm) [78] |
| HQEtСP | Tb [72] Eu,Tb [73] |  |  |  |
| HQAd | Tb [81] |  |  |  |
| HQNB | Tb [82] |  |  |  |
| HQC11 | Dy [83] |  |  |  |
| HQC15 | Tb [84]; Eu [85]; Dy [86] |  |  |  |
| HQC17 | Eu, Gd Tb[87]; Tb, Y [88]; Tb [37] |  | 21800 [87] 21980 [37] |  |
| HQCF3 | Eu, Tb[89]; Yb, Gd [90]; La, Nd, Eu, Gd, Tb, Er, Yb [91]; La, Yb, Gd [92]; La, Nd, Gd, Er, Yb [93]; La, Nd, Gd, Er, Yb [94], Nd, Er, Yb [95]; La, Nd, Eu, Gd, Tb, Er, Yb [96] | 31000[90] 27027 [91] 27027 [92] 25126 [93] 26667 [94] | 18832 [90] 18975 [91] 18795 [92] 18727 [93] 19268 [94] | 4.89*104 (249, 289) [94] |
| HQPh | Tb, Gd [39]; Dy [97]; Eu [98]; Eu [99]; Eu [69]; Eu [100]; Eu, Tb, Ho, Er, Tm [101]; Tb, Ho, Er, Tm [102]; Eu, Tb [103]; Eu [104]; Nd, Er, Yb [105]; Yb [106]; Nd [107]; Dy [83]; Dy [86]; Tb [61] | 35700 [106] | 21000 (19340)a [39] | 5.14*104 (253 nm) [39] |
| HQ3,5Me2C6H3 | Nd [108] |  |  |  |
| HQp-C6H4Me | Eu [109]; Tb [40] |  |  |  |
| HQp-C6H4Ph | Eu [109] |  |  |  |
| HQp-C6H4tBu | Yb, Gd [43]; Er [110] |  | 21300 (19230)a [43] |  |
| HQp-C6H4NMe2 | Eu, Gd [47] | 24450 [47] | 20900 (19900)a [47] | 5.5*104 (360 nm) [47] |
| HQp-C6H4NC | Eu, Gd [47] | 27027 [47] | 20300 (18200)a [47] | 3.5*104 (301 nm) [47] |
| HQC6F5 | Sm, Eu, Gd, Tb, Lu [32] |  |  | ~1.5*105 M-1cm-1 (293 nm) [32] |
| HQ1-Nh | Eu, Gd [47]; Tb [40] | 28900 [47] | 21100 (19600)a [47] | 6.1*104 (288 nm) [47] |
| HQO | Tb [89] |  |  |  |
| HQS | Eu, Tb [89]; Eu, Tb, Gd [74]; Eu [111] |  | 20800 (n.d.)a [74]; |  |
| HQCH2Ph | La, Pr-Yb [89] |  |  |  |
| HQ5-COOHPy | Eu, Tb [112] |  |  |  |
| Proligands with R1 ≠Ph and/or R2 ≠ Me |  |  |  |  |
| HQ2-Py,Me,CF3 HQ2-Py,Me,Ph HQ2-Py,Me,p-C6H4F HQ2-Py,Me,CH2Ph HQ2-Py,Me,2-Nh | Eu [113] |  |  |  |
| HQ3-ClC6H4,Me,3,5Me2C6H3 | Nd [108] |  |  |  |
| HQ4-MeC6H4;Me;3,5Me2C6H3 | Nd [108] |  |  |  |
| HQpMeC6H4,Me, C3F7 | Tb [40] |  |  |  |
| HQp-NCPh,Me,iPr | Tb3+ [114] | 28600 [114] | 24150 [114] | 9.18*104M-1cm-1 (286 nm) [114] |
| HQPh,2-Py,Ph | Gd [115] |  | 20200(18300)a[115] |  |
| HQPh,2-C4H3S,Ph | Gd [115] |  | 19400(16400)a[115] |  |
| HQPh,CF3,Me | Tb [116] |  |  | (300nm) |
| HQPh,Ph,Me | Yb3+ [117] |  |  |  |
| HQPh,Ph,CH2Ph | Tb, Gd [30] | 31150[30] | 21050 [30] | 7.8*104 (264 nm) [30] |
| HQPh,X1,CH2Ph с | Tb, Gd [30] | 31550[30] | 21050 [30] | 7.6*104 (261 nm) [30] |
| HQPh,X2,CH2Ph с | Tb, Gd [30] | 31850[30] | 21050 [30] | 8.4*104 (274 nm) [30] |
| HQPh,X3,CH2Ph с | Tb, Gd [30] | 33200[30] | 21080 [30] | 10.0*104 (275 nm) [30] |
| Proligands H2QRQ c |  |  |  |  |
| H2Q1Q | Tb,Eu, Gd [118]; Y, La, Pr, Nd, Sm-Yb [119] |  | 22989 [118] |  |
| H2Q2Q | Tb,Eu, Gd [118]; Y, La, Pr, Nd, Sm-Yb [120]; Tb [121] |  | 23148 [118] |  |
| H2Q3Q | Tb,Eu, Gd [118]; Dy [122]; Y, La, Pr, Nd, Sm-Yb [123]; La, Pr, Nd, Sm-Yb [124]; Tb [125]; Sm [126] |  | 23419 [118] |  |
| H2Q4Q | Tb,Eu, Gd [118]; Tb [127]; Y [128]; Dy [129]; Tm [130]; Sm [131]; Lu [132]; Tb [133] |  | 23319 [118] |  |
| H2Q7Q | Tb,Eu, Gd [118] |  | 21978 [118] |  |
| H2Q8Q | Tb,Eu, Gd [118]; Tb, Gd [134] | 32939 [134] | 21930 [118] 23201 [134] |  |
| H2Q1,3Q | Ce [135] |  |  |  |
| H2Q1,4Q | Ce [135] |  |  |  |
| H2QPyQ | Eu, Tb [136] |  |  |  |
| H3Q1,3,5QQ | La [137] |  |  |  |

a  - In these cases, the energy value of the triplet level is given according to the spectra published in the article using the tangent method; the energy value proposed in the original article is given in parentheses.

b - Given for [LnQ3(solv)n] complexes.

c – The molecular structures of the proligands are depicted in scheme 1.

Scheme 1. Structures of some acylpyrazolones, see Table 1.

The acylpyrazolones in the neutral form exhibit at least five tautomeric forms (Scheme 2).

Scheme 2. Tautomeric forms of HQ proligands.

Tautomerism is possible both in solution and in the solid state. The primary forms for 4-acylpyrazol-5-ones are 1 and 2. The enolic form 1 predominates in CHCl3 solution and when dissolved in other weakly polar and nonpolar solvents, due to stabilization by intramolecular hydrogen bonding. Crystallization from CHCl3 also occurs in this form. The amino-diketone form 2 is stabilized in polar solvents due to a network of N–C∙∙∙O bonds and crystallizes from them. Additionally, the phenyl radical at the C3 position stabilizes form 2. Some acylpyrazolones are capable of crystallizing in form 4 [138–141].

When acylpyrazolones react with lanthanides they exhibit properties of monobasic acids, dissociating one proton [17,18]. Coordination typically occurs through both atoms of the β-diketonate group, provided there are no steric hindrances. Coordination modes of acylpyrazolones in complexes with various s-, p-, d-, and f-metals have been described in a review [17]. In most lanthanide compounds, acylpyrazolonates demonstrated chelating properties, coordinating a single metal atom (Scheme 3, (a)); however, coordination via a chelate-bridging type is also possible (Scheme 3, (b)). The (c) type of coordination was found in {AgLnQCY4} heterometallic complexes, with silver atoms exclusively bonded to the nitrogen atoms of the pyrazole rings [80]. There are reports describing acylpyrazolones also coordinated in the neutral form in [LnQPh3(NO3)3] complexes, as inferred from IR spectra [142], or from the combination of IR data with quantum calculations [143], but confirming X-ray data are lacking.

Scheme 3. Coordination modes of HQ ligands realized in Ln3+ complexes.

Since acylpyrazolones behave as monobasic acids, it is theoretically possible to obtain coordination compounds with different charges: [Ln(Q)n]+3-n, n =1-4. In practice, neutral complexes of the composition [Ln(Q)3] and anions [Ln(Q)4]- have been reliably described, while coordination of only one or two acylpyrazolonate ligands is feasible in the presence of an additional ligand that forms a strong bond with the lanthanide, such as a β-diketonate. There are reports of complexes [LnQPh2(NO3)(X)], where X is a monodentate O-donor ligand [144], but single crystal diffraction data for such compounds are lacking. Since acylpyrazolonate is a rather bulky ligand, the coordination numbers (CN) of lanthanides in acylpyrazolonates are usually 7-8, the most reported species being the octahedral seven-coordinated neutral [Ln(Q)3(L)] and the eight-coordinated neutral [Ln(Q)3(L)2] and anionic [Ln(Q)4]-, where L is a neutral ligand [17].

In most lanthanide acylpyrazolonates to date investigated, the proligands employed are 1-phenyl-3-methyl-acylpyrazolones with a substituent in the 4-position (Scheme 4).

Scheme 4. Structures of the most common HQ ligands.

We propose the following classification for lanthanide acylpyrazolonates based on composition of the metal's coordination sphere, charge of the complex, and presence of additional ligands:

- Neutral complexes incorporating solvent molecules into the coordination sphere: [Ln(Q)3(solv)n].

- Monoligand neutral complexes [Ln(Q)3]2.

- Heteroleptic neutral complexes [Ln(Q)3(L)n], containing an additional neutral ligand.

- Anionic complexes M[Ln(Q)4], where M is a monovalent cation.

- Polynuclear complexes with chelating and bridging acylpyrazolonates.

- Complexes with bisacylpyrazolonates (typically binuclear compounds forming a triple helix structure [Ln2(QRQ)3(L)n], as well as the only structurally characterized anionic complex [Na(DB-18-Crown-6)(H2O)][Ln(Q8Q)2] [134].

Tris-solvates [LnQ3(solv)1-2]

Lanthanide acylpyrazolonates, where the metal ions are additionally coordinated by solvent molecules, represent the most common class. Given that rare-earth cations typically exhibit high coordination numbers (CN), and acylpyrazolonates are bidentate ligands, the central atom additionally coordinates solvent molecules, increasing the CN to 7 or, more frequently, 8. No exceptions to this rule have been found so far; however, the structure of a samarium complex with a neutral methylated acylpyrazolone ligand QPh,Me,(Me),CH2Cl has been identified (Figure 1), indicating the potential for increasing the CN of lanthanides in acylpyrazolonates to nine under specific conditions [145]. For scandium, which has a small ionic radius, it is possible to form anhydrous tris-complexes [ScQ3] with a coordination number of 6 [146], although in other cases it reaches 7 upon coordination with a solvent molecule [78]. The complexes of the type [LnQ3(solv)1-2] described to date are listed in Table 2.

Figure 1. Structure of the ligand QPh,Me,(Me),CH2Cl and of the complex [Sm(QPh,Me,(Me),CH2Cl)3(H2O)4](ClO4)3 [145].

The synthesis of complexes with lower coordination numbers is impossible in the presence of solvents containing N- or O-donor atoms. This explains the large number of examples of eight-coordinated complexes described in the literature: when neutral compounds are synthesized in common solvents such as H2O, EtOH, and DMF, it is impossible to avoid their incorporation into the coordination sphere without introducing additional ligands.

The main methods for synthesizing tris-solvate complexes are presented in Scheme 5. The classical synthetic scheme for lanthanide acylpyrazolonates is as follows: 3 equivalents of the ligand are dissolved in ethanol (in some cases, CHCl3 is used). Then, 1 equivalent of lanthanide chloride, nitrate, or perchlorate and 3 equivalents of a base are added to the solution to neutralize the acidity of the ligand. The inorganic salt of the alkali metal with the lanthanide salt anion precipitates out and is separated from the mother liquor. Lanthanide acylpyrazolonates in solid form were obtained after evaporation of the solvent. An alternative method can be used to obtain solvates with aprotic solvents such as THF by using Ln[N(SiMe2)]3 as starting reagent.

Scheme 5. [LnQ3(solv)1-2] synthesis.

In neutral [LnQ3(solv)1-2], lanthanides compounds have generally coordination numbers (CN) ranging from 7 to 8, upon coordination by six oxygen atoms from the acylpyrazolones and one or two solvent molecules. When CN is 8, the most commonly realized polyhedra are the square antiprism and the bicapped trigonal prism, exhibiting various degrees of distortion (Figure 2). It is possible in the case of two independent structures for a single complex to exist as different polyhedra [147]. The polyhedron is primarily determined by the size of the ligand, with the contribution of substituents to the resulting structure being influenced solely by steric factors rather than their chemical nature [148][72].

A CN of 7 occurs less frequently and is observed in selected cases involving sterically hindered ligands, such as  the anionic QCP [72] (Figure 3) and QCY  [75] [76]. Interestingly, for the latter ligand, the boundary between CN 7 and 8 for tris-complexes lies between Sm and Eu [77], which is attributed to lanthanide contraction.

Figure 2. The two different coordination polyhedra of Tb found in [Tb(QMe)3(H2O)2] [147]: (a) the square antiprism, (b) the bicapped trigonal prism.

Figure 3. (a) The heptacoordinated complex [TbQCP3(H2O)] and (b) the capped trigonal prismatic coordination polyhedron of Tb3+ [72].

Table 2. Lanthanide tris(acylpyrazolonate) solvate complexes: CN, synthetic methods and luminescence properties.

| Complex | CN, polyhedron | Luminescent properties | Method of synthesisa | Ref. | Year |
| --- | --- | --- | --- | --- | --- |
| LnQPh3*xH2O, Ln=Y, Pr-Er, x=3; Ln=Yb, x=1 | n/a | n/a | 1 | [100] | 1985 |
| [EuQs3(H2O)(EtOH)] | 8 | n/a | 1 | [111] | 2003 |
| [YbQPh,Ph,Me3(H2O)2]*3EtOH | 8 | n/a | 1 | [117] | 1987 |
| [LnQCH2Ph3(H2O)(EtOH)], Ln=La,Pr, Nd, Sm-Yb | 8 |  | 1 | [89] | 2002 |
| [LnQCH2Ph3(H2O)2], Ln=La, Lu | 8 | Ln=Eu PLQY 0.02%, τ 95µs Sm PLQY 0.12% | 1 | [89] | 2002 |
| [LnQS3(H2O)(EtOH)], Ln=Eu, Tb | 8 | n/a | 1 | [89] | 2002 |
| [TbQ03(H2O)(EtOH)] | 8 |  | 1 | [89] | 2002 |
| [TbQCF3(H2O)2] | 8 |  | 1 | [89] | 2002 |
| [DyQCH3(H2O)2]*0.375CH3COOC2H5 | 8 | PLQY 1.2%, τ 12.75 µs | 1 | [38] | 2018 |
| [DyQPh3(H2O)2]*CH3CN | 8 |  | 1 | [97] | 2021 |
| [GdQiPr(H2O)2GdQiPr3(C2H5OH)(H2O)] |  |  | 1 | [41] | 2006 |
| [TbQCP3(H2O)(EtOH)] | 8 | n/a | 1 | [72] | 2003 |
| [TbQEtCP3(H2O)(EtOH)]*2EtOH | 8 | n/a | 1 | [72] | 2003 |
| [TbQCP3(H2O)] | 7 | n/a | 3 | [72] | 2003 |
| [TbQEtCP3(H2O)] | n/a | n/a | 3 | [72] | 2003 |
| [TbQp-NCPh,Me,iPr3(H2O)(EtOH)] | n/a | n/a | 1 | [114] | 2021 |
| [LnQC173(H2O)(EtOH)], Ln=Eu, Gd, Tb | 8 | Eu – only at 77K, τ 332 µs Tb τ 610 µs (77K and 300K) | 1 | [87] | 2014 |
| [YQC173(H2O)2] [TbQC173(H2O)(EtOH)] | 8 | Tb τ 897 µs (solid state) τ 498-583 µs (hybrid materials) τ 601 µs (grafted film) | 1 | [88] | 2015 |
| [TbQC173(H2O)2](H2O)3 | n/a | 626 µs (solid state) LB films also studied | 1 | [37] | 2018 |
| [LnQCH2tBu3(H2O)2], Ln=Tb, Gd | 8 | Tb-centered | 1 | [65] | 2004 |
| [LnQCY3(H2O)(EtOH)](EtOH), Ln=Sm, Pr, Nd | 8 | Pr 0.4% (IR) Nd PLQY 1.3% (IR region) Sm 1.3% (visible)+0.5 (IR) | 1 | [77] | 2023 |
| [LnQCY3(H2O)], Ln=Eu, Gd | 7 | Only at 77K τ 90 µs | 1 | [75] | 2021 |
| [LnQCY3(H2O)], Ln=Dy, DyxGd1-x LnQCY3(D2O)], Ln=Dy, DyxGd1-x | 7 | 1.4% for Ln=Dy, H2O 1.7% for Ln=Dy0.25Gd0.75, H2O 2.1% for Ln=Dy, D2O 2.7% for Ln=Dy0.1Gd0.9, D2O | 1 | [76] | 2022 |
| [LnQCY3(H2O)], Ln=Sc, Gd, Lu [LuQCY3(DMSO)] [LaQCY3(H2O)(EtOH)] | 7 7 8 | Greenish phosphorescence of Gd complex and blue fluorescence of all other compounds | 1 | [78] | 2023 |
| [LnQC6F53(THF)] | n/a | Only ligand-centered emission | 2 | [32] | 2015 |
| Nd(QPh;Me;3,5Me2C6H3)3(H2O)(EtOH) | n/a | Visible area. Judd-Ofelt analysis | 1 | [108] | 2023 |
| Nd(Q3-ClC6H4;Me;3,5Me2C6H3)3(H2O)(EtOH) | 8, SAPR | Visible area Judd-Ofelt analysis | 1 | [108] | 2023 |
| Nd(Q4-MeC6H4;Me;3,5Me2C6H3)3(H2O)(EtOH) | n/a | Visible area Judd-Ofelt analysis | 1 | [108] | 2023 |
| [TbQC15)3(EtOH)] | n/a | τobs(Tb) 900 µs LB films also studied | 1 | [84] | 1999 |
| [TbQC15)3(EtOH)] | n/a | τobs(Tb) 702 µs (solid), 62 µs (CH2Cl2 solution) LB films also studied | 1 | [133] | 1997 |
| EuQPh3*4H2O | n/a | 380 µs (300K) 750 µs (77K) | 1 | [69] | 2000 |
| EuQCH2Cl3*4H2O | n/a | 300 µs (300K) 420 µs (77K) | 1 | [69] | 2000 |
| [LnQ5-COOHPy3(H2O2)], Ln=Tb, Eu | n/a | Spectra given only for Tb complex. Used as turn off sensor for Bovine serum albumin | 1 | [112] | 2012 |
| [Ln(QPh,Ph,CH2Ph)3(H2O)(EtOH)], Ln = Gd, Tb | 8 | PLQY 0.10%, τ 2.4 µs | 1 | [30] | 2006 |
| [Ln(QPh,X1,CH2Ph)3(H2O)2], Ln = Gd, Tb | 8 | PLQY 0.43%, τ 49.6 µs | 1 | [30] | 2006 |
| [Ln(QPh,X2,CH2Ph)3(H2O)], Ln = Gd, Tb | n/a | PLQY 1.11%, τ 404.7 µs | 1 | [30] | 2006 |
| [Ln(QPh,X3,CH2Ph)3(H2O)], Ln = Gd, Tb | n/a | PLQY 2.26%, τ 389.4 µs | 1 | [30] | 2006 |
| [LnQ1-Nh3(H2O)2], Ln=Eu, Gd | n/a | PLQY 0.92 %, τ 31.50 µs | 1 | [47] | 2005 |
| [LnQC6H4p-NMe23(H2O)2], Ln=Eu, Gd | n/a | PLQY 0.31 %, τ 18.57 µs | 1 | [47] | 2005 |
| [LnQC6H4p-CN3(H2O)2], Ln=Eu, Gd | n/a | PLQY 0.04 % | 1 | [47] | 2005 |
| [LnQi-Pr3(H2O)2], Ln=Eu, Gd | n/a | n/a | 1 | [47] | 2005 |
| [EuQp-C6H4Me3(EtOH)] | n/a | n/a | 1 | [109] | 2015 |
| [EuQp-C6H4Ph3(H2O)2](H2O)] | n/a | n/a | 1 | [109] | 2015 |
| [LnQCF33(H2O)2], Ln=La, Nd, Gd, Er, Yb | 8, SAPR | τ 1.33 µs (Ln=Nd) τ 15.8 µs (Ln=Yb) | 1 | [94] | 2014 |
| [GdQCF33(H2O)2] | n/a |  | 1 | [90] | 2022 |
| [TbQiPr3(H2O)(EtOH)] | n/a | Green luminescence | 1 | [56] | 2003 |
| [TbQPh3(H2O)2] | n/a | Weak green luminescence in DMF solution | 1 | [61] | 1998 |
| [TbQiPr3(H2O)2] | n/a | τ 483 µs (DMF) | 1 | [61] | 1998 |

a Methods 1 and 2 are described in the scheme 4; method 3 is a vacuum heating of corresponding hydrate or re-crystallization from Me2CO.

Complexes containing no solvate solvents and additional ligands (anhydrous complexes)

To date, only a few anhydrous rare-earth acylpyrazolonates have been reliably characterized (See Table 3). This is due to the fact that the six oxygen donor atoms of the three Q- anions cannot coordinatively saturate these ions. The nitrogen atoms of the pyrazole rings, which could potentially complement the coordination sphere of Ln3+ and facilitate the formation of a polymeric structure, are too soft for hard Pearson acids such as the rare-earth cations. For a long time, the only reliably studied complex of this type remained [Tb2Qp-NCPh,Me,iPr6], whose dimeric structure is formed by the coordination of nitrile groups of the p-C6H4CN substituent at the R1 position of the ligand [114] (Figure 4, (a)). In 2012, L.N. Bochkarev et al. found a way to synthesize binuclear anhydrous complexes [Ln2Q6] with common proligands such as HQiPr and HQtBu. These compounds were obtained by reacting metallic Ln with the HQ ligand in a THF medium in the presence of an activator (anhydrous LnI3 or I2) [46] [62]. In these structures, the anionic Q- exhibits chelate-bridging coordination (Figure 4, (b)). Removal of solvents from the coordination sphere of the metal improves luminescent properties compared to tris-solvate complexes.

Figure 4. Structures of anhydrous acylpyrazolonates:  (a) [Tb2Qp-NCPh,Me,iPr6] Hydrogen atoms omitted for clarity [114] and (b) [Ln2QtBu6], hydrogen atoms and C6H5 groups omitted for clarity [62].

This series of compounds can be supplemented by the complex [CeQ4ClC6H4,Ph,S4], described as a toluene solvate. This compound is a unique example of an acylpyrazolonate of cerium in the +4 oxidation state and is described by the authors as an air-stable compound [16].

Table 3. Monoacylpyrazolone complexes: anhydrous complexes.

| Complex | CN, polyhedron | Luminescent properties | Method of synthesis | Reference, Year |
| --- | --- | --- | --- | --- |
| [ScQPh3] | 6, octahedron | n/a | 3HQ+Sc(NO3)3, MeOH/H2O | [146], 1997 |
| [Tb2Qp-NCPh,Me,iPr6] | 7 | PLQY 97.1% (solid state); 32.6 (MeOH solution). MeOH – 32.6%, τ 942 µs CD3OD – 48.6%, τ 1837 µs Solid – 97.1%, τ 561 µs Doped film 98.9%, τ 824 µs OLED also tested | Vacuum sublimation of [TbQ3(H2O)(EtOH)] | [114], 2002 |
| [LnQtBu3], Ln=Tb, Gd, Tb0.01Gd0.99, Tb0.05Gd0.95 | n/a | Tb: τ 160 µs (295K), 980 µs (78K) PLQY 12% | Thermal decomposition on [LnQ3(bipy)] in vacuo | [64], 2002 |
| [Ln2QiPr6], Ln=Y, Nd, Gd, Tb, Er, Tm, Lu | 7, Capped trigonal prism |  | Ln0 + 3HQ, THF, I2 or LnI3 (cat), vacuum drying | [46], 2012 |
| [Ln2QtBu6], Ln=Pr, Nd, Gd, Tb, Tm, and Lu | 7, Capped trigonal prism |  | Ln0 + 3HQ, THF, I2 (cat), vacuum drying | [62], 2013 |
| [Tb2QtBu6] | n/a | PLQY 4.41% (CH2Cl2] | Ln0 + 3HQ, THF, I2 (cat), vacuum drying | [58], 2012 |
| [TbQiPr2QNB]2 | n/a | PLQY 1.61% (CH2Cl2) | 1. 2Na(DME)QiPr+TbCl3 (THF) 2. Na(DME)QNB, THF | [82], 2014 |
| [CeQ4ClC6H4,Ph,S4](C6H5CH3) | 8, dodecahedral | n/a |  | [16], 2014 |

Adducts with Aromatic Diimines and Related Ligands

The primary drawback of tris-hydrate complexes is their reduced luminescence intensity, which is caused by quenching due to the vibrations of O-H bonds in water or alcohol molecules. Replacing these molecules with a bidentate nitrogen-donor ligand enhances the luminescent properties and thermal stability of the complexes, which accounts for their extensive variety in the literature. The synthesis of these complexes is typically conducted similarly to the preparation of tris-solvates but in the presence of a diimine ligand (Scheme 6). Alternatively, in a pre-synthesized tris-solvate complex solvent molecules can be substituted. In all cases where X-ray structural analysis data are available, the coordination number of the lanthanide in such complexes is 8. The complexes of this class described to date are listed in Table 4.

Table 4. Monoacylpyrazolone Complexes – Adducts with bipy, phen, etc. ligands.

| Formula | CN, polyhedron | Luminescent properties | Ref. | Year |
| --- | --- | --- | --- | --- |
| [TbQC173(bipy)], Ln= Tb | n/a | 857 µs (300K) LB films also studied | [37] | 2018 |
| [LnQCF33 bipy], Ln= La, Nd, Gd, Eu, Tb, Er, Yb | 8 | ФNdNd = 1.27% ФLNd = 0.068% ФYbYb = 1.35% ФLYb = 1.12% ФErEr = 0.13% ФLEr = 0.002% Luminescence of Eu and Tb complexes are weak; for Nd and Yb OLED fabricated | [91] | 2016 |
| [YbQCF33 (bipy)] | 8, SAPR | ФYbYb = 0.81% Hybrid materials with PMMA | [92] | 2015 |
| [LnQAd3(bipy)], Ln=Eu, Tb | 8 | Eu and Tb emission | [81] | 2006 |
| [LuQi-Pr3(bipy)] | n/a | OLED fabricated | [49] | 2003 |
| [LnQtBu3(bipy)], Ln = Tb, Gd | n/a | n/a | [64] | 2002 |
| [YbQCF33(bipy)] | 8, square antiprism | electroluminescence | [90] | 2022 |
| [TbQAd3(bipy)] | 8, square antiprism | intensive green luminescence | [81] | 2006 |
| [TbQPh3(bipy)] | n/a | Weak in DMF solution | [61] | 1998 |
| [TbQiPr3(bipy)] | n/a | 520 µs (DMF) | [61] | 1998 |
| [LnQPh3(Me2bipy)]·EtOH, Ln= Tb, Ho, Tm, Er | 8, triangular dodecahedron | Ln3+ emission | [102] | 2023 |
| [LnQPh3(MEO2bipy)], Ln= Eu, Tb, Ho, Tm, Er |  |  | [101] | 2024 |
| [LnQCH2tBu3(5Br-bipy)], Ln= Sm, Gd, Tb | 8, square antiprism | white-light emission ФLTb = 36% ФLSm = 5.2% | [66] | 2022 |
| [LnQCH2tBu3(5Br-bipy)], Ln=La, Sm, Gd | n/a | White light (Ligand + Sm emission) OLED fabricated | [67] | 2020 |
| [LnQCF33(phen)], Ln=La, Nd, Gd, Er, Yb | 8, square antiprism | ФNdNd = 1.11% ФNdL = 0.90% ФYbYb = 1.37% ФYbL = 1.06% For Er weak emission; for Yb OLED fabricated | [93] | 2016 |
| [LnQAd3(phen)], Ln=Eu, Tb | 8 | Eu and Tb emission | [81] | 2006 |
| [LnQCP3(phen)], Ln=Eu, Tb | ? | Eu and Tb emission at 77K | [73] | 2004 |
| [LnQEtCP3(phen)], Ln=Eu, Tb | ? | Eu and Tb emission at 77K | [73] | 2004 |
| [TbQCH2tBu3(phen)]·CHCl3 | 8 | Tb emission | [65] | 2004 |
| EuQPh3(phen)*2H2O | n/a | Eu emission, τ 1000 µs (77k) | [69] | 2000 |
| EuQCH2Cl3(phen)*2H2O | n/a | Eu emission, τ 790 µs (300) | [69] | 2000 |
| [LnQPh3(phen)], Ln=Eu, Tb | n/a | Eu and Tb emission Temperature dependance | [103] | 2015 |
| [LuQi-Pr3(phen)] | n/a | Ligand emission OLED fabricated | [49] | 2003 |
| GdQi-Pr3(phen) | n/a | Green phosphorescence (528 nm) OLED fabricated | [52] | 2002 |
| [YbQCF33(phen)] | 8, square antiprism | NIR emission OLED fabricated | [90] | 2022 |
| [TbQi-Pr3(phen)2 | n/a | PLQY 1.57% (CH3CN) OLED |  |  |
| [TbQiPr3(phen)] | n/a | Tb emission OLED fabricated | [55] | 2002 |
| [Eu(TTA)2(QC6H4-p-tBu)(Phen)] |  | Eu emission OLED fabricated | [149] | 2000 |
| [LnQPh,Me,p-tBuPh3(bath)], Ln= Yb, Gd | n/a | 18.0 µs (300K), OLED | [43] | 2012 |
| [LnQCP3(bath)], Ln=Eu, Tb | ? | Eu and Tb emission at 77K | [73] | 2004 |
| [LnQEtCP3(bath)], Ln=Eu, Tb | ? | Eu and Tb emission at 77K | [73] | 2004 |
| [YbQCF33(bath)] | 8, square antiprism | NIR emission OLED fabricated | [90] | 2022 |
| LnQPh3(L)], L=PhenX, PhenY, Ln=Eu, Tb | n/a | Eu and Tb emission + Temperature dependance | [103] | 2015 |
| [TbQPhCF3Me3(TDZP)] | 8, square antiprism | Tb emission OLED fabricated | [116] | 2018 |
| [LnQCHEt23(BIMZ)], Ln=La, Gd, Tb | n/a | For Tb green emission, τ 258 µs | [70] | 2017 |

Scheme 6.  N-donor additional ligands.

Complexes with phosphine oxide ligands and phosphoric acid derivatives as additional ligands

Oxygen-donor ligands based on phosphine oxides and related compounds constitute an alternative to nitrogen-donor ancillary ligands. These compounds having generally stoichiometry [LnQ3(O=PR3)n], n=1-2 are listed in Table 5. The interest towards these ligands is due to the use of trialkyl phosphates or their mixtures with diketone ligands, including acylpyrazolone ligands, for the extraction separation of lanthanides [14,15,104]. The most common complexes are those with triphosphine oxide, which, due to steric hindrance, sometimes stabilizes a coordination number of 7 for the central atom. The reduction in the symmetry of the environment leads to a partial lifting of the electronic transition restrictions, which improves the photo- and electroluminescent properties of the complexes. Therefore, some of these compounds have been tested in OLED devices.

From this perspective, the complexes [LnQiPr3(TPPO)2] and [LnQtBu3(TPPO)] have been actively investigated, as they can exhibit luminescence in the visible region, especially for terbium and dysprosium, as well as in the IR region, and even for non-emitting rare earth elements (Y, Lu, Gd) due to ligand fluorescence and phosphorescence [40,42,45,48–51,53,54,56,57].

The bisphosphine oxide ligands dppMO2, dppEO2, and dppBO2 were employed by our group with the aim to synthesize luminescent coordination polymers. It was shown that in the case of the ligand dppMO2, monomeric [LnQR3(dppMO2)] complexes are formed where the phosphine oxide exhibits chelate coordination, whereas increasing the number of methylene units in the P-donor ligand to 2 or 4 leads to the formation of chain coordination polymers {LnQR3(dppXO2)}   [150] (Figure 5).

Figure 5.  Synthesis of complexes LnQ3(dppxO2) with monomeric (x=CH2) and polymeric (x=(CH2)2 and (CH2)4) structure [150].

Table 5. Monoacylpyrazolone Complexes: Adducts with Phosphine Oxides and Related Ligands.

| Complex a |  | CN, polyhedron |  | Luminescent properties |  | Method of synthesis |  | Ref. |  | Year |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| [EuQPh3(O=P(OiBu)3)2] |  | 8 |  | Eu3+ emission |  | EuQ3(H2O)2+2L, EtOH |  | [104] |  | 1983 |  |
| [Dy(Qi-Pr)3(TPPO)2] |  | 8, Dist. Bicapped trigonal prism |  | PLQY 3.5% τobs 17.6 µs Judd-Ofelt analysis |  | 1LnCl3+3HQ+3NaOH, EtOH |  | [44] |  | 2013 |  |
| [Sm(Qi-Pr)3(TPPO)2] |  | n/a |  | PLQY 2.7% τobs 84.7 µs Judd-Ofelt analysis |  | 1LnCl3+3HQ+3NaOH+2TPPO, EtOH |  | [42] |  | 2008 |  |
| [LnQC6F53(TPPO)] |  | 7 |  | Only Eu and Sm shows Ln-centered emission |  | [LnQC6F53(THF)]+TPPO (CHCl3) |  | [32] |  | 2015 |  |
| [Eu(Qi-Pr)3(TPPO)2] |  | Dist. Triang. Dodecahedron |  | n/a |  | 1LnCl3+3HQ+3NaOH+2TPPO, EtOH |  | [45] |  | 2005 |  |
| [LnQi-Pr3(TPPO)2] |  | n/a |  | 24.9 µs (300K) NIR-OLED |  | 1LnCl3+3HQ+3NaOH+2TPPO, EtOH |  | [43] |  | 2012 |  |
| [LnQ3(TPPO)] |  | 7 |  | green luminescence |  | 1LnCl3+3HQ+3NaOH+1TPPO, EtOH |  | [65] |  | 2004 |  |
| [LnQR3(dppMO2)], R=S, CP; Ln=Eu, Gd, Tb |  | 8, SAPR |  | Eu and Tb emission + Temperature dependance |  | 1Ln(NO3)3+3HQ+3NEt3+1dppMO2, EtOH, r.t. |  | [74] |  | 2010 |  |
| {LnQR3(X)}, R=S, CP; Ln=Eu, Gd, Tb; X=dppEO2, dppBO2 |  | 8, SAPR |  | Eu and Tb emission + Temperature dependance |  | 1Ln(NO3)3+3HQ+3 NEt3+1dppXO2, EtOH, autoclave (130o, 6h) |  | [74] |  | 2010 |  |
| [EuQ1-Nh3(TPPO)(H2O)] |  | n/a |  | OLED fabricated |  | 1 |  | [47] |  | 2005 |  |
| [EuQC6H4-p-NMe23(TPPO)(H2O)] |  | n/a |  |  |  | 1 |  | [47] |  | 2005 |  |
| [EuQC6H4-pCN3(TPPO)(H2O)] |  | 8, SAPR |  |  |  | 1 |  | [47] |  | 2005 |  |
| TbQi-Pr3(TPPO)2 |  | n/a |  | Used as ETL in OLED, Tb-centered emission also observed |  | n/a |  | [48] |  | 2002 |  |
| [LuQi-Pr3(TPPO)2] |  | 8, Bicapped trigonal prism |  | Blue fluorescence; OLED fabricated |  | 1 |  | [49] |  | 2003 |  |
| [DyQi-Pr3(TPPO)2] |  | 8, Bicapped trigonal prism |  | τ 7.24 µs PLQY 3.5% OLED fabricated |  | 1 |  | [50] |  | 2007 |  |
| [ErQi-Pr3(TPPO)2] |  | 8, Bicapped trigonal prism |  | τ 3.3 µs Judd-Ofelt OLED fabricated |  | 1 |  | [51] |  | 2008 |  |
| [NdQi-Pr3(TPPO)2] |  | n/a |  | τ 2.2 µs Judd-Ofelt OLED fabricated |  | 1 |  | [53] |  | 2009 |  |
| [TbQi-Pr3(TPPO)2] |  | n/a |  | OLED fabricated |  | 1 |  | [54] |  | 1998 |  |
| [TbQMe3(TPPO)2] |  |  |  | PLQY 5.84% (CH3CN) OLED |  |  |  | [40] |  | 1999 |  |
| [TbQEt3(TPPO)2] |  |  |  | PLQY 7.31% (CH3CN) OLED |  |  |  | [40] |  | 1999 |  |
| [TbQnPr3(TPPO)2] |  |  |  | PLQY 6.76% (CH3CN) OLED |  |  |  | [40] |  | 1999 |  |
| [TbQi-Pr3(TPPO)2] |  |  |  | PLQY 13.91% (CH3CN) OLED |  |  |  | [40] |  | 1999 |  |
| [TbQOEt3(TPPO)2] |  |  |  | PLQY 16.21% (CH3CN) OLED |  |  |  | [40] |  | 1999 |  |
| [TbQt-Bu3(TPPO)] |  |  |  | OLED |  | n/a |  | [63] |  | 2000 |  |
| [TbQCHEt23(TPPO)] |  | 7, capped trigonal prism |  | OLED |  | 1 |  | [71] |  | 2003 |  |
| [TbQi-Pr3(TPPO)2] |  | n/a |  | OLED |  | 1 |  | [56] |  | 2003 |  |
| [TbQCHEt23(TPPO)] |  | n/a |  | OLED |  | 1 |  | [56] |  | 2003 |  |
| [TbQi-Pr3(TPPO)2] |  | n/a |  | τ 223.2 (298K) PLQY 14.6% (CH2Cl2) OLED |  | 1 |  | [57] |  | 2009 |  |
| [TbQi-Pr3(DPPOC)] |  | n/a |  | τ 204.7 (298K) PLQY 16.7% (CH2Cl2) OLED |  | 1 |  | [57] |  | 2009 |  |
| [TbQiPr2QNB(TPPO)2] |  | n/a |  | PLQY 2.40% (CH2Cl2] |  | 1 |  | [82] |  | 2014 |  |
| [LnQS3(EtOH)(LP), Ln = Eu, Sm |  | 8, SAPR |  | n/a |  | 1 |  | [68] |  | 2013 |  |
| [Ln(QnPe)3(EtOH)(LP)], Ln=Tb, Dy |  | n/a |  | Emission spectra |  | 1 |  | [68] |  | 2013 |  |
| [TbQi-Pr3(TPPO)2] |  | n/a |  | Emission spectra |  | 1 |  | [60] |  | 1998 |  |

a See scheme 7.

Scheme 7.  Phosphine oxide and phosphate-based additional ligands.

Tetrakis acids and their derivatives

Another method to reduce vibrational quenching is to move from neutral tris-pyrazolonate complexes to acid tetrakis pyrazolonates X+[LnQ4]-. In such compounds, substituted ammonium ions, hydroxonium ions H3O+ [76], and Zundel ions H5O2+ [151] can serve as X+ cations. The isolation of alkali metal salts had long been unsuccessful [75]; however, using the HQH proligand, analogous complexes have been also obtained. The presence of nitrogen donor atoms in the pyrazole ring of acylpyrazolones makes them potentially suitable to yield heterometallic complexes with soft cations such as Ag+, usable in the synthesis of silver-containing tetrakis-complexes {AgLnQCY4} with a polymeric structure [80]. Anionic lanthanide complexes M[LnQ4] are listed in Table 6.

The synthesis of tetrakis-complexes can be conducted using the classical method 1 with an excess of the HQ proligand or by a cleaner "hydroxide" method [75,76,80], where pre-precipitated Ln(OH)3 is washed and dissolved in an excess of the HQ ligand. Cation substitution can be achieved through exchange reactions; however, it should be noted that at least in the case of the HQCY ligand, tris-complexes are thermodynamically more stable, and any heating of the solution leads to the irreversible decomposition of tetrakis-complexes [75,76] according to the equation:

H3O+[LnQCY4-]  + H2O  [LnQCY3(H2O)1-2] + HQCY

Table 6. Anionic Lanthanide Complexes.

| Complex | CN, polyhedron | Luminescent properties | Method of synthesis | Reference, year |
| --- | --- | --- | --- | --- |
| {H3O}+[Ln(QH)4]-.nH2O, Ln=Nd, n=2; Sm, n=3; Eu, Tb, n=1 | 8, SAPR | Studied PLQY: Sm – 0.75% Eu -0.08% Tb – 27.9% | 4HQ+1Ln(NO3)3+3NaOH, EtOH 96% | [34], 2013 |
| Na+[Ln(QH)4]-, Ln=Nd, Sm, Eu, Tb | 8 |  | 4HQ+4NaOH+1Ln(NO3)3, EtOH | [36], 2013 |
| [NBu4]+[Ln(QH)4]-, Ln=Nd, Sm, Eu, Tb | 8 | All compounds at r.t. | 4HQ+4NaOH+1Ln(NO3)3+1NBu4I, EtOH | [36], 2013 |
| (A)+[Dy(QPh)3(QC16)]- |  |  | B+I-+Dy(NO3)3+4HQ, EtOH | [86], 1995 |
| (A)+[Dy(TTA)3(QC16)]- |  |  | B+I-+Dy(NO3)3+3HTTA+HQ, EtOH | [86], 1995 |
| H3O[Tb(QC17)(QH)3]- | n/a | 651 µs (300K) LB films also studied | TbQH(H2O)2+HQ, EtOH | [37], 2018 |
| {H3O}+[Tb(QC17)4]- | n/a | 513 µs (300K) LB films also studied | 4HQ+3NaOH+Ln(NO3)3, EtOH | [37], 2018 |
| [NBu4]+[Ln(QCH2Ph)4]-, Ln=Tb, Eu | 8 |  | 5HQ+1NBu4I+5KOH+1Ln(NO3)3, EtOH | [89], 2002 |
| {H5O2}+[Ln(QCY)4]- | 8, SAPR | Eu – only at 77K Tb at r.t. | 4HQ+1Ln(NO3)3+3KOH, EtOH | [151], 2006 |
| {H3O}+[Ln(QCY)4]-, Ln=Dy, DyxGd1-x {D3O}+[Ln(QCY)4]-, Ln=Dy, DyxGd1-x | 8 | ~3% for Ln=Dy, H2O and D2O, decrasing for Ln=DyxGd1-x | Ln(OH)3+4.25HQ, EtOH, r.t. | [76], 2021 |
| {H3O}+[Ln(QCY)4]-, Ln=Pr, Nd, Sm | 8 | PLQY 1.3% (Nd) 0.4% (Pr) 2.0 (visible) + 0.4 % (IR) - Sm | Ln(OH)3+4.25HQ, EtOH, r.t. | [77], 2023 |
| {H3O}+[Ln(QCY)4]-, Ln=Sm, Eu, Gd, Tb, Dy | 8, SAPR |  |  | [80], 2023 |
| {AgLn(QCY)4}, Ln=Sm, Eu, Gd, Tb, Dy | 8, SAPR |  |  | [80], 2023 |
| [NBu4]+[Ln(QCF3)4]-, Ln=Tb, Eu | 8 | Ln=Tb, PLQY 0.4% | 5HQ+1NBu4I+5KOH+1Ln(NO3)3, EtOH | [89], 2002 |
| {H3O}+[Ln(QS)4]-, Ln=Tb, Eu, Lu | 8, SAPR | n/a | 3.05HQ+1Ln(NO3)3+3KOH, EtOH (traces) 4HQ+1Ln(NO3)3+3KOH, EtOH (main product) | [111], 2003 |
| (B)+[Dy(QPh)4]- | n/a | n/a | n/a | [83], 1994 |
| (B)+[Dy(QPh)3(QC11)] - | n/a | n/a | n/a | [83], 1994 |
| (C)+[Eu(QPh)4]- | n/a | LB films |  | [98], 1994 |
| (A)+[Dy(QPh)4]- |  |  | B+I-+Dy(NO3)3+4HQ, EtOH | [86], 1995 |
| (D)+[Nd(QPh)4]- | n/a | OLED fabricated | n/a | [107], 1996 |
| (D)+[ [Yb(QPh)4]- | n/a | LB-films |  | [106], 1997 |
| [(CnH2n+1)2NMe2]+[Eu(QPh)4]-, n=14, 16, 18 | n/a | LB-films | 4HQ+1LnCl3+4NaOH+1NR4Br, EtOH. Recryst. From MeOH | [99], 1997 |
| [NBu4]+[Eu(QPh)4]-*3H2O | n/a | 390 µs (300K) 930 µs (300K) | 1Ln(NO3)3+4HQ+4KOH+NBu4I, EtOH | [69], 2000 |
| (E)+[Ln(QPh)4]-, Ln=La, Nd, Er, Yb | 8, SAPR | CH3CN solutions 10-5 M: Nd τ 1.0 µs Er τ 3.2 µs Yb τ 46.4 µs | 4HQ+1LnCl3+4NaOH+1NDDMS+Br-, EtOH, recryst. EtOH+H2O | [105], 2007 |

Legenda:

Bisacylpyrazolones

The use of halogenated anhydrides of dicarboxylic acids as precursors in the Jensen reaction opened the way to a new type of ligands – bisacylpyrazolones. The ligands most investigated are the H2QnQ derivatives, where n corresponds to the polymethylene bridging group –(CH2)n–. In comparison to monoacylpyrazolonates, this class of ligands is characterized by much less study via X-ray crystallography of single crystals. Apparently, in most cases, the most common product is a triple helicate [Ln2(QnQ)3(solv)m], where for n=2 the coordination number of the lanthanide reaches only seven (Figure 6, (a)) [121]. An increase of C atoms in the bridge, produces a decrease in the rigidity of the fragment, allowing a coordination number of 8 to be achieved at m=2 (Figure 6, (b)) [122,125,126]. Further increasing the length of the bridge allows the ligand to "bend" and to form a chelating anionic complex of the type [Ln(Q8Q)2]-, reported as a salt with the cation [Na-DB-18-Crown-6]+ (Figure 6, (c)) [134]. Data on lanthanide bisacylpyrazolonates are systematized in Table 7.

Figure 6. Molecular structures of the complexes bisacylpyrazolones [Tb2(Q2Q)3(H2O)2] [121], (a), B [Dy2(Q3Q)3(DMF)4] [122] (b), and [Na-DB-18-Crown-6][Tb(Q8Q)2]-  [134] (c). Hydrogen atoms and outer-sphere solvent molecules are omitted for clarity.

The luminescent properties of bisacylpyrazolonates have been also studied indirectly, but H2QnQ ligands have been proposed as analytical reagents for fluorimetric determination of a number of lanthanides, including Tm3+ ions [130], whose blue emission sensitization in the visible range is usually a challenging task.

Table 7. Bis-acylpyrazolonate complexes.

| Complex a | CN, polyhedron | Luminescent properties | Method of synthesis | Reference | Year |
| --- | --- | --- | --- | --- | --- |
| Ln2(Q1Q)3(H2O)10, Ln=Eu, Gd, Tb | n/a | ITb>>IEu | 2Ln(NO3)3+3H2QQ+6NaOH, EtOH | [118] | 2014 |
| [Ln2(Q1Q)3(phen)2]*nH2O, Ln=Y, n=6 La, n=3 Pr, Nd, Sm, Eu, Gd, Tb, Dy, Ho, Er, Tm, Yb n=4 | n/a | Nd, Gd, Ho – only ligand emission; Pr, Sm, Eu, Tb, Dy, Tm – Ln3+ emission | 2H2QQ+1.16Ln(NO3)3+1Phen+4NaOH, EtOH | [119] | 1993 |
| [[Ln2(Q2Q)3(phen)2]*nH2O, Ln=Y, Pr-Lu n=4; Ln=La, n=5 | n/a | Pr, Sm, Tb, Dy, Tm | 1.05LnCl3+1.5H2QQ+1Phen+3NH3(aq) | [120] | 1990 |
| [Tb2(Q2Q)3(H2O)2] | 7+7, mono-capped octa- hedron | PLQY 18% (EtOH) | Tb(NO3)3+H2QQ+Et3N, 1700C, autoclave | [121] | 2008 |
| [Tb2(Q2Q)3(dmf)2] | 7+7, mono-capped octa- hedron |  | Recrystallization of [Tb2(Q2Q)3(H2O)2] from DMF | [121] | 2008 |
| {Tb2(Q2Q)3(dppEO2)}n | 7+7, mono-capped octa- hedron |  | [Tb2(Q2Q)3(dmf)2] + dppEO2, DMF, | [121] | 2008 |
| Ln2(Q2Q)3(H2O)5, Ln=Eu, Gd, Tb | n/a | ITb>>IEu | 2Ln(NO3)3+3H2QQ+6NaOH, EtOH | [118] | 2014 |
| [Ln2(Q3Q)3(bipy)n(H2O)m] Ln=Y, n=2, m=2 La, n=1, m=10 Pr, Nd, Sm n=1, m=3 Eu-Yb, n=2, m=4 | n/a | ITb>ISm>IDy | 1LnCl3+2bipy+1.5H2QQ+3NaOH, EtOH | [123] | 1994 |
| (CTA)+[Ln(Q3Q)2]-, Ln=Y, La-Nd, Sm-Yb | n/a | Pr, Sm, Eu, Tb, Dy – Ln centered, other – ligand emission | 1LnCl3+2H2QQ+1.2CTAB+4NaOH, EtOH | [124] | 1992 |
| Ln2(Q3Q)3(H2O)6, Ln=Eu, Gd, Tb | n/a | Observed only for Tb complex | 2Ln(NO3)3+3H2QQ+6NaOH, EtOH | [118] | 2014 |
| Tb2(Q3Q)3(H2O)6 | n/a | n/a | 2Ln(NO3)3+2H2QQ+4NaOH, EtOH | [125] | 1994 |
| [Tb2(Q3Q)3(DMF)4](dmf) | 8+8 (SAPR) | n/a | Recrystalization of Tb2(Q3Q)3(H2O)6 from DMF | [125] | 1994 |
| Sm2(Q3Q)3(H2O)7 | n/a | n/a | 2Ln(NO3)3+2H2QQ+4NaOH, EtOH | [126] | 1995 |
| [Sm(Q3Q)3(DMF)4](dmf) | 8+8 (SAPR) | n/a | Recrystalization of Sm2(Q3Q)3(H2O)7 from DMF | [126] | 1995 |
| Dy2(Q3Q)3(H2O)2 | n/a | n/a | 2Ln(NO3)3+2H2QQ+4NaOH, EtOH | [122] | 1996 |
| [Dy(Q3Q)3(DMF)4](dmf) | 8+8 (SAPR) | n/a | Recrystalization of Dy2(Q3Q)3(H2O)2 from DMF | [122] | 1996 |
| (CTA)+[Sm(Q4Q)2]- | n/a | Sm-centered emission | It was not isolated in pure form, but was used for the selective determination of Sm3+in solution. | [131] | 1995 |
| (CTA)+[Lu(Q4Q)2]- | n/a | Ligand emission at 438 nm | It was not isolated in pure form, but was used for the selective determination of Lu3+in solution. | [132] | 1997 |
| [C16H33NMe3]+[Y(Q4Q)2] | n/a | Fluorescence, λmax446 nm | It was not isolated in pure form, but was used for the selective determination of Y3+ in solution. | [128] | 1994 |
| (E)+[Dy(Q4Q)2] | n/a | n/a | 1Dy(NO3)3+2H2QQ+4NaOH+1Base:, EtOH-H2O | [129] | 1994 |
| (CTA)+[Tm(Q4Q)2]- | n/a | Tm-centered emission at 478 nm | It was not isolated in pure form, but was used for the selective determination of Tm3+in solution. | [130] | 1995 |
| [NMe2(C18H37)2][TbQ4Q)2] | n/a | τobs(Tb) 727 µs (solid), 792 µs (CHCl3 solution) | 2.2 H2QQ+1Ln(ClO4)3+4NaOH+ 1[NMe2(C18H37)2]Br, EtOH | [133] | 1997 |
| Ln2(Q4Q)3(H2O)4, Ln=Eu, Gd, Tb | n/a | ITb>>IEu | 2Ln(NO3)3+3H2QQ+6NaOH, EtOH | [118] | 2014 |
| [C16H33NMe3][Tb(Q4Q)2] | n/a | Spectra | It was not isolated in pure form, but was used for the selective determination of Tb3+in solution. | [127] | 1994 |
| Ln2(Q7Q)3(H2O)4, Ln=Eu, Gd, Tb | n/a | ITb>>IEu | 2Ln(NO3)3+3H2QQ+6NaOH, EtOH | [118] | 2014 |
| Ln2(Q8Q)3(H2O)4, Ln=Eu, Gd, Tb | n/a | ITb>>IEu | 2Ln(NO3)3+3H2QQ+6NaOH, EtOH | [118] | 2014 |
| [Ln2(QPyQ)3(H2O)4], Ln=Eu, Tb | n/a | Eu, Tb at r.t. | LnCl3+1.5H2QQ+3NaOH, EtOH | [136] | 2010 |
| [Ln2(Q8Q)3(H2O)2], Ln=Tb, Gd | n/a | Tb – PLQY 4.82% τ 1110 µs | 2Ln(NO3)3+3H2QQ+6NaOH, EtOH | [134] | 2008 |
| [Na(DB-18-Crown-6)(H2O)]+[Ln(Q8Q)2]-, Ln=Tb, Gd | 8, SAPR | Tb – PLQY 18.13% τ 2820 µs | 1Ln(NO3)3+2H2QQ+4NaOH + 1 DB-18-Crown-6, EtOH | [134] | 2008 |

a The elements whose complexes were investigated by single-crystal X-ray diffraction method are highlighted in bold.

Legenda

Heterometallic d-f complexes based on rare earth acylpyrazolonates

As noted earlier, the presence of donor nitrogen atoms in the structure of lanthanide acylpyrazolonates makes them potentially suitable for the synthesis of heterometallic complexes. Currently, there are only two examples in the literature of the formation of such structures, where the transition metal cations are Ag+ [80] and [L2Ir]+ [113] cations.

It has been shown that heterometallic silver complexes can be obtained by mixing solutions of complex acids H3O[Ln(QCY)4] (Ln = Sm, Eu, Gd, Tb and Dy) with a silver nitrate solution in the presence of NEt3 as a base [80]. In this case, polymeric salts of {Ag[Ln(QCY)4]}n are formed. These compounds were fully characterized by elemental analysis, FTIR spectroscopy, SCXRD and PXRD. It has been found that the silver ion in such compounds is associated with three acylpyrazolonate residues (Figure 7). The formation of {Ag[Ln(QCY)4]}n significantly reduces the LMCT-quenching of Eu3+, which is characteristic of this system, and has virtually no effect on the luminescence of Sm3+, Tb3+, and Dy3+ ions.

Figure 7. Fragment of the crystal packing {Ag[Gd(QCY)4]}n (phenyl, cyclohexyl and methyl groups are omitted for clarity) [80].

The introduction of [L2Ir]+ fragments into the structure of lanthanide acylpyrazolnates is an example of the search for an effective antenna able to sensitize the luminescence of lanthanide ions [113]. In this case, the acylpyrazolone itself acts as a linker ligand for excitation energy transfer. To identify the possibility of energy transfer and the effect of the triplet level of the linker ligand on the efficiency of this transfer, a series of complexes {[L2Ir(Q2-Py,Me,R)]3EuCl}Cl2 (L = (2,4-difluoro)phenylpyridine, R = CF3, Ph, Bn, 4F-Bn and 2-Naph) were synthesized, where the substituent was changed at the carbonyl group of acylpyrazolone (Figure 8). Complexes in Figure 8 were synthesized by refluxing [L2Ir(Q2-Py,Me,R)] with EuCl3·6H2O in ethanol, the obtained precipitates being recrystallized from CH2Cl2/n-hexane and characterized by elemental analysis, HRMS, FTIR, 1H NMR and NEXAFS spectroscopy. In order to obtain an efficient energy transfer the triplet level of the linker ligand should be sufficiently lower than the 3MLCT energy levels of the Ir moiety and higher than the resonance level of the lanthanide ion.

Figure 8. Structural formula of complexes {[L2IrQ2PyMeR]3EuCl}Cl2 [113].

The linker ligand may not be present at all when the excitation energy is transferred to the lanthanide ion. In this case, the antenna, which is a transition metal complex, is directly coordinated to the lanthanide ion. There are two examples in the literature of the formation of such complexes, where zinc acts as the transition metal [(4-R-Py)Zn(L)Ln(QCF3)3] (Figure 9, L - N,N’-bis(salicylidene)cyclohexane-1,2-diamine, R = H, Ln = La, Nd, Yb, Er, Gd, R = Vi, Ln = La, Nd, Yb, Er, Gd, Eu, Tb) [95,96]. Such compounds are obtained by mixing solutions of [(4-R-Py)Zn(L)] complexes with solutions of tris-solvates and then refluxing the mixtures. IR-emitting ions in such coordination environment are sensitized most effectively, and their complexes can be used to create highly effective hybrid luminescent materials based on PMMA.

Figure 9. Molecular structures of (a) [PyZn(L)Yb(QCF3)3] [95] and (b) [(4-vi-Py)Zn(L)Eu(QCF3)3] [96]. Hydrogen atoms and solvent molecules are omitted for clarity.

Luminescent properties of REE acylpyrazolonates

The luminescence of lanthanide complexes typically occurs according to the Weissman antenna sensitization mechanism [9,12] and is described within the framework of the modified Jablonski-Crosby diagram [11,13,152]. In the initial stage, the organic antenna ligand absorbs a quantum of light and transitions to an excited singlet state (S*). Through internal conversion, the molecule then moves to a long-lived triplet state (T*), from which energy is transferred to the Ln3+ ion. This mechanism circumvents the primary obstacle to creating efficient lanthanide-containing luminophores—namely, the weak extinction coefficients of Ln3+ ions [11,13,153]

It appears that the luminescence of lanthanide acylpyrazolonates was first described by Emiliya Toivovna Karaseva and colleagues, who worked in Vladivostok (USSR) in the 1970s [14,15,154]. They recorded emission spectra of complexes of the type [Ln(QPh)3(H2O)2] and  [Ln(QPh)3(O=P(O-iBu)3)2] for Ln = Sm, Eu, Tb, and demonstrated that low-temperature (77K) emission spectra contain only bands corresponding to transitions within the 4f-shell of lanthanides. This indicates that the anionic QPh ligand can sensitize the luminescence of Ln3+.

Three reasons can be proposed to explain why the next surge of interest in the emission properties of lanthanide acylpyrazolonates occurred only a decade later, in the 1990s. First, the triplet level energy of the most accessible HQPh ligand is unsuitable for sensitizing terbium and dysprosium emissions at room temperature due to the proximity of the triplet level energy to the resonance levels of these ions. Second, for europium ions, a luminescence quenching mechanism via LMCT (Ligand-to-Metal Charge Transfer) states is realized, leading to the unusual effect where the quantum yield of samarium derivatives exceeds that of europium ions. Both ions have similar resonance level energies; however, in most cases, europium complex emissions are very intense due to the ease of non-radiative deactivation of the Sm3+ ion emitting in the visible and IR regions. However, for Eu3+, the LMCT mechanism is most prevalent due to its electrochemical potential E0(Eu3+/Eu2+ = –0.35 V [155]). Quenching occurs because the Q- anion can act as a reductant. The third reason is the explosive growth of interest in OLED technologies in the 2000s and the discovery of terbium-containing acylpyrazolone emitters in the late 1990s by Gao et al. [54,56]

The energy relationship between the resonance level of Ln3+ and the triplet level energy of ligands plays a crucial role in antenna sensitization of lanthanide luminescence. The energy of these levels is provided in Table 1, along with singlet levels and molar extinction coefficients where available in the literature. The determination of the triplet energy levels of a ligand is usually carried out by using low-temperature phosphorescence spectra of Gd3+ complexes [11,156–158] because they are often isostructural to complexes of other lanthanides, and they exhibit a significant spin-orbit interaction that increases the efficiency of phosphorescence. This phenomenon is referred to as the "paramagnetic effect" [157].  However, this method for determining triplet level energies is characterized by several difficulties, without careful consideration of which, data accuracy is questionable:

- It is essential to specifically record phosphorescence spectra, which means that the registration should occur after a certain time interval (several µs) following the excitation impulse. Otherwise, both fluorescence and phosphorescence of the ligand will be present in the spectrum, and the value of the triplet energy level may be significantly overestimated.

- In cases of low intensity or poor resolution of the spectra, one can switch from studying pure solid complexes to examining their frozen solutions in glass-forming solvents such as EtOH [114][113], EtOH:MeOH 1:1 [113],  EME (EtOH:MeOH:Et2O 8:2:1) [157] or EPA (Et2O:isopentane:EtOH 5:5:2)  mixtures [12].

- When using heteroligand complexes, it is necessary to ensure that the triplet level of the additional ligand lies significantly higher than that of the investigated ligand [159]. In general, it is better to use tris-solvate complexes or tetrakis-anions with optically inactive cations. The results of triplet level measurements for tris- and tetrakis-complexes do not differ [76,80].

- Spectra should be presented in an energy representation, i.e., converting from wavelength to energy, and intensities should be corrected by multiplying for the square of the wavelength.

- A uniform method for determining the 0-0 transition should be used. The determination of its exact value is extremely difficult, but its energy corresponds not to the maximum in the phosphorescence spectrum [12], but to the high-energy Gaussian component. It can be assumed that the Gaussian decomposition method will give an underestimated value, while the tangent method will give an overestimated one. However, for comparing data, it is important to use the same methodology for different compounds. For this reason, we did not simply summarize literature data, but in cases where the original phosphorescence spectra of Gd3+ complexes were provided in the studies, we digitized the spectral data and re-evaluated the triplet energy levels using the tangent method [158]. For example, the triplet level of the HQPh ligand reported in [39] as 19,340 cm-1 indicates that this ligand is not capable of sensitizing the luminescence of Tb3+ ions (5D4 energy about 20,400 cm-1[11]), although it had been previously observed, albeit with low quantum yields [14,61,154], and an estimate of  21,000 cm-1 seems more realistic.

The triplet energy levels of most acylpyrazolones lie in the range of 20,000 to 24,000 cm-1. For ligands with R1=Ph and R2=Me, the influence of the substituent at position R3 can be described as follows:

- For all aliphatic substituents at R3, the most reliable T* data fall within the range of 22,500-24,500 cm-1, which is suitable for efficient sensitization of Tb3+ and Dy3+ luminescence. The sensitization of samarium luminescence is less effective due to the high gap compared to the excited state energy of samarium at 17,400 cm-1 [11]. The same applies to Eu3+ ions, but the observed lower efficiency of Eu3+ complex luminescence compared to Sm3+ is likely due to LMCT quenching of the former [75,80];

- For aromatically substituted ligands HQPh, HQS, and HQ1-Nh, the triplet energy levels are significantly lower but still exceed the resonance level energy of the 5D4 state of Tb3+ ions (20,400 cm-1). As a result, terbium complexes with these ligands exhibit luminescence upon cooling, which is associated with the suppression of back thermal energy transfer. The luminescence efficiency of Eu3+ and Sm3+ complexes with these ligands is generally higher than that of lanthande acylpyrazolonates with aliphatic substituents.

- For the two other ligands of this type, namely HQH and HQCF3, the triplet energy levels are 20,700 and 18,800 cm-1, respectively. This makes the former more promising as a sensitizer for the luminescence of samarium, europium, and IR-emitting ions.

To identify the patterns in the changes of the ligand's energy features based on its structure, we attempted to plot a dependence of the triplet energy level of HQR ligands on various substituent R characteristics to reveal any regularities. The most illustrative dependence was found to be on the parameter F, which can be calculated using Hammett constants σm and σp [160]:

F=1.297 σm-0.385 σp+0.033

The graph is presented in Figure 10:

Figure 10. Dependence of the triplet energy level of ligands on the parameter F. The most reliable values of the triplet level, as indicated in Table 1, are shown. The values of parameter F are taken from reference [160]. In the right part of the figure, the energies of the emission levels of some Ln3+ ions are presented. The shaded rectangles demonstrate the optimal energy gaps for the sensitization of terbium luminescence (green) and europium luminescence (red) [12,156].

The data on the graph is insufficient for a confident analysis. Additionally, it is important to remember that the values of triplet energy levels should be determined under identical conditions and using the same methodology. Nevertheless, in Figure 10, we observed a decrease in triplet energy with increasing F. Furthermore, there is a clear distinction between two clusters, marked in green and red, containing aliphatic and aromatic substituents.

Triplet energy levels for only a few ligands with substituents R1 ≠ Ph or R2 ≠ Me have been investigated [30,114,115]. The comparison of ligands HQp-NCC6H4,Me,iPr and HQiPr shows a coincidence of triplet energy levels ([114]  vs 23,900-24,500 cm-1 [39,41,43]; respectively), which is not surprising, as the substituent in the phenyl ring is quite remote. However, replacing the donor methyl substituent R2 with an aromatic one (2-Py or 2-Thi) [115] leads to a significant decrease in the triplet energy level by 800-1700 cm-1, with the thiophene-containing ligand demonstrating a lower triplet state energy. Increasing the size of the dendrimer system of substituents in ligands HQPh,Ph,CH2Ph, HQPh,X1,CH2Ph, HQPh,X2,CH2Ph and HQPh,X3,CH2Ph  does not have a measurable effect on the triplet energy levels, although it allows for a slight increase in the molar absorption coefficients for these ligands [30].

The analysis of data on the luminescence of lanthanide acylpyrazolonates indicates that this class of ligands serves as an effective luminescence sensitizer. This is most prominently found in terbium compounds, where quantum yields approaching 100% are achievable [114]. For dysprosium ions, the energy of the resonance level (~20,833 cm-1) is quite similar to that of terbium (~20,408 cm-1), and the same ligands can sensitize the emission of both ions [11,76,152]. However, due to the complex structure of the energy levels, the quantum yields of dysprosium derivatives are consistently lower than those of their terbium counterparts. The dysprosium compounds exemplify several strategies to enhance luminescent characteristics. For instance, the transition from hydrates to adducts with phosphine oxide increases the photoluminescence quantum yield (PLQY) from 1.2-1.4% [38,76] to 3.5% [44]. A similar effect is achieved by replacing light water molecules with their heavy counterpart D2O [76]. Additionally, suppressing concentration quenching when transitioning from monometallic dysprosium complexes to bimetallic systems DyxGd1-x allows for an approximate 1.5-fold increase in quantum yield. The PLQY for the tetrakis acid [H3O][Dy(QCY)4] is 3%, exceeding that of the tris-complex [Dy(QCY)3(H2O)]  by a factor of two; however, methods involving gadolinium dilution or substitution of the H3O+ cation with D3O+ do not yield significant effects [76].

Luminescence of europium complexes with acylpyrazolones is often not very efficient, which is attributed to LMCT quenching, as discussed earlier. Evidence of such quenching can be a strong temperature dependence of the luminescence of europium complexes; for example, in some cases it appears only at the temperature of liquid nitrogen and is low-intensity at room temperature  [75,150,161,162].  Recently, we demonstrated the presence of a luminescence-quenching CT state for Ln=Eu during the study of excitation spectra and diffuse scattering for the complexes {AgLnQCY4} and [H3O][Eu(QCY)4] (Figure 11), wherein silver cations partially suppress this side process [80]. For samarium complexes, the quantum yield of luminescence can exceed 5% when an appropriate triplet-level ligand is utilized and quenching oscillators are removed [66].

Figure 11. PL excitation spectra of complexes H3O[LnQCY4] and {AgLnQCY4}n pairwise. In the case of europium complexes, an intense band corresponding to the LMCT state is observed, which is suppressed in the case of the silver-containing polymer [80].

Infrared-emitting ions such as Pr3+ [77,94], Nd3+ [53,77,91,93,94,105], Er3+ [51,91,93,94,105], and Yb3+ [90–93,105] can exhibit metal-centered luminescence in acylpyrazolonates, particularly when employing the aforementioned strategies to suppress vibrational quenching using phosphine oxide [51,53], pyridyl [90–93]  ligands, or tetrakis acid derivatives [77,105].

Applications of Lanthanide Acylpyrazolonates

Extraction and Separation of Rare Earth Elements (REEs).

The first area of application for acylpyrazolone ligands in REE chemistry pertains to their use in extraction separation. For many years since the pioneering work by Jensen [2], the extraction and separation of trivalent lanthanides by acylpyrazolones are of great relevance and interest [5,163–165]. The solvent extraction of Ln3+ by acylpyrazolone (HQ) [166] can be expressed by the following equation (where a = aqua, o = organic):

Ln3+ (a) + 3HQ(o)  LaQ3(o) + 3H+(a).

The equilibrium constant Ka is calculated as:

Ka = D[H+]3[HQ]-3,       where D = [LnQ3]o/[Ln3+]a.

The ligands (HQ) with lower pK values have been found to extract metal ions from more acidic solutions. Due to the high CN of Ln3+, the complex to be formed contains two additional water molecules that makes it sufficiently hydrophilic to ensure a greater solubility in water than in a non-polar solvent favoring a low extraction coefficient. At higher concentrations of HQ, LnQ3HQ complexes can be extracted. The extraction ability of REE by acylpyrazolones decreases with increase of ionic radius of Ln3+ due to the HSAB theory. This property can be used for REE separation.

The extraction of Ln3+ is masked by fluoride, oxalate, phosphate and EDTA that form more stable complexes. For the same reason Ce4+ lowers the extraction up to 81% [167].

The mechanistic studies of MQ3 complex formation at toluene-water interface indicate that formation and dissociation reactions of MQ3 occur exclusively at the phase boundary and are catalyzed by Arsenazo III complex formation in the aqueous phase through its adsorption at the interface [168].

To enhance the extraction, a combination of HQ with neutral monodentate or bidentate donor ligand S is used that demonstrated the synergistic effect [168–174]. The typical ligands S are organophosphorus esters, alkylphosphine oxides and sulfides, alkyl phosphonates, substituted monothiophosphinic acid, primary amine, 1,10-phenanthroline (Phen) etc. In the presence of S, the overall synergic reaction proceeds as follows:

Ln3+(a) + mHQ(o) + nS(o) = LnQ3nS(o) + mH+(a)

Ksyn = Dsyn[H+]m/[HQ]m[S]n, where Dsyn = D – Do,

Ksyn being the mixed equilibrium constant when n = 1 or 2.

A synergism occurs due to the replacement of coordinated water by S molecules. At lower concentration, one water molecule is replaced by S while at higher concentration, both water molecules are replaced by S. In a strong acid medium the anation takes place, giving mixed ligand species [LnQ2XB], where X is a nitrate or perchlorate group [175,176].

The synergistic enhancement factor for the mixture of HQ and monodentate organophosphorus ligand is nearly 2, e.g. for La3+ with HQPh  and triisobutylphosphine sulfide it is calculated to be 1.82 [176]. The use of neutral tripodal ligands on the triphenylphosphine oxide platform with anchored carbamoyl side arms gives a strong enhancement of synergistic effect up to 107[177].

The process of liquid-liquid extraction of Ln3+  by HQ in liquid paraffin with cersin has been developed. The results showed that increasing temperature is favorable to extraction of heavy rare earth ions with HQPh and to synergistic extraction with (QPh)- and Phen [176].

OLED emitting layers

The second, chronologically, but most significant in terms of importance, is the use of lanthanide acylpyrazolonates in the creation of luminescent materials, particularly for the development of emitting and auxiliary layers in OLED devices. Data on detailed OLED devices based on lanthanide complexes are presented in Table 8. Moreover, a number of early articles containing almost no quantitative characteristics of electroluminescence are not mentioned in the table XXX.

The first OLED devices based on neodymium and dysprosium acylpyrazolonates were developed nearly 30 years ago in 1996, utilizing Langmuir-Blodgett films of the complexes (E)[Ln(QPh)4] (for (E)+ structure see legenda of table 6) with cations containing extended alkyl substituents [107,178]. The broad luminescence bands of these compounds were attributed to transitions within the organic part of the complex, while transitions of the f-elements were not observed. Just two years later, the terbium complex [TbQi-Pr3(TPPO)2] was proposed as an effective luminescent material  [54,60]. It has been shown that complexes of this type have good electron transport properties in addition to electroluminescence [60]. Terbium complexes are the most extensively studied due to their superior photoluminescent properties, particularly with aliphatic substituents on the R3 position of the ligands, compared to other rare earth elements (REEs). Furthermore, several elements have been tested with similar complexes of the type [LnQi-Pr3(TPPO)2] and have been demonstrated suitable for both lanthanide ions that emit in the visible range (Tb3+ [48,56,60], Dy3+ [50]) and for IR-emitting ions (Nd3+ [53], Er3+ [51], Yb3+ [43]), as well as for optically neutral Lu3+ ions [49] where only ligand luminescence is feasible. Metal-centered electroluminescence has been observed even in single-layer devices [47,54,56,63,71,179], and the introduction of additional layers along with material optimization significantly enhances device performance. For some OLED devices, efficiency characteristics approaching record levels of external quantum efficiency (EQE 14.8% [180]) and brightness (6300 [116], 18500 [56], [71] 20000  cd.m2 ) have been achieved.

An interesting approach has been proposed by selected studies, where improved electroluminescent characteristics are attained through the use of multiple emitting layers containing either identical or different terbium acylpyrazolonates [56] [57] [180] or ytterbium derivatives[43].  It has been suggested that a dual-layer device combining two distinct acylpyrazolonates of rare earth ions exhibited optimal characteristics due to a more effective balance of charge carriers in the active region[43].

In addition to their application in emitting layers, in several cases, Ln3+ acylpyrazolonates, mainly [GdQiPr3(TPPO)2] [59] and [YQiPr3(bipy)] [181] have been successfully employed as transport layer materials.

Table 8. Some OLED devices containing rare earth acylpyrazolonates as emission layers.

| Complex |  | OLED structurea | Lambda max, emission color | Perfomance, cd*m2 (Voltage, V), Turn on voltage | Irradiance, mW/cm2 | Ref., Year |
| --- | --- | --- | --- | --- | --- | --- |
| Y-based OLEDs |  |  |  |  |  |  |
| [Y(QiPr)3(bipy)] |  | ITO/PVK (40 nm)/ Complex (80 nm)/Mg:Ag (200 nm)/Ag (100 nm) | Green (502 nm) | 177 (20V) |  | [181] 2001 |
|  |  | ITO/PVK (40 nm)/ Complex (40 nm)/ALQ (40 nm)/Mg:Ag (200 nm)/Ag (100 nm) | Green (510 nm) | 1750 (15V) |  |  |
|  |  | ITO/ Complex (40 nm)/ALQ (40 nm)/Mg:Ag (200 nm)/Ag (100 nm) |  | 147 (16V) |  |  |
|  | Nd-based OLEDs |  |  |  |  |  |
| (E)[NdQPh4] |  | ITO/Complex (29-80 nm)/Al | 570-668 nm | (4V) |  | [107] 1996 |
| (E)[NdQPh4] |  | ITO/Complex (29-80 nm)/Al | 500-700 nm | Turn on 4-7V |  | [178] 1996 |
| [Nd(Qi-Pr)3(TPPO)2] |  | ITO/NPB(20 nm)/Complex (50nm)/AlQ (30 nm) /LiF/Al 150 (nm) | IR (1060 nm) | (19.2) | 0.98(341) | [53] 2009 |
|  |  | ITO/NPB(15 nm)/Complex (55nm)/BCP (15 nm)/AlQ (35 nm) /LiF/Al 150 (nm) |  | (16.5) Turn on 8.1V | 2.1 |  |
| Sm-based OLEDs |  |  |  |  |  |  |
| [Sm(QCH2tBu)3L], L= 5-Br-2,2′-bipy |  | ITO:(PEDOT:PSS)/PVK@Complex/TPBI/LiF:Al | White light (422 nm + 651 nm) | 157 (10) |  | [67] 2022 |
| Eu-based OLEDs |  |  |  |  |  |  |
| [Eu(TTA)2(QC6H4-p-tBu)(Phen)] |  | ITO/TPD/Complex/AlQ/Mg:Ag | Red, 615 nm | 16 Turn on 9V |  | [149] 2000 |
| [Eu(Q1-Nh)3(TPPO)(H2O)] |  | ITO/Complex (60 nm)/Mg:Ag10:1 (200 nm)/Ag (80 nm). | No emission |  |  | [47] 2005 |
|  |  | ITO/NPB (50 nm)/ Complex:CBP (6%, 50 nm)/AlQ (40 nm)/Mg:Ag10:1 (200 nm)/Ag (80 nm) | Yellow (502 nm wide+615 nm (sharp) | 920 (n/a) |  |  |
|  |  | ITO/NPB (50 nm)/ Complex:CBP (15%, 50 nm)/ BCP (20 nm)/AlQ (20 nm)/Mg:Ag10:1 (200 nm)/Ag (80 nm) | Red (615 nm) | 247 (18.5) |  |  |
| Gd-based OLEDs |  |  |  |  |  |  |
| [Gd(Qi-Pr)3(phen)] |  | ITO/TPD(20 nm)/ Complex (65 nm)/ Mg: Ag(200 nm)/Ag(100 nm) | Green (535+406+422 nm) | 126(13) |  | [52] 2002 |
|  |  | ITO/TPD(20 nm)/ Complex (80 nm)/BCP(20 nm)/Mg: Ag(200 nm)/Ag(100 nm) |  | 230(17) Turn on 5V |  |  |
| Tb-based OLEDs |  |  |  |  |  |  |
| [Tb2(Qp-NCPh,Me,iPr)6] |  | ITO:MoO3(2nm)/MoO3(25nm, 20%):mCp(15nm)( DCPPO:Complex(20nm, 15%) /DPEPO(10 nm)/TPBi(30nm)/LiF(1nm)+Al(100 nm) | Green (543 nm) | 774 (4.1) |  | [114] 2021 |
|  |  | ITO:MoO3(2nm)/MoO3(25nm, 20%):mCp(15nm)( DCPPO:Complex(20nm, 15%) /DPEPO(10 nm)/TPBi(50nm)/LiF(1nm)+Al(100 nm) | Green (543 nm) | 971 (4.1) |  |  |
|  |  | ITO:MoO3(2nm)/MoO3(25nm, 20%):mCp(15nm)( DCPPO:Complex(40 nm, 15%) /DPEPO(10 nm)/TPBi(50nm)/LiF(1nm)+Al(100 nm) | Green (543 nm) | 1383 (4.7) |  |  |
| [Tb(QiPr)3(TPPO)2] |  | ITO/TPD(40nm)/CBS(20nm)/Complex(60nm)/Al | Greenish-blue |  |  | [48] 2002 |
|  |  | ITO/TPD(40nm)/CBS(30nm)/Complex(50nm)/Al | Blue | 253 (19) |  |  |
|  |  | ITO/TPD(40nm)/CBS(40nm)/Complex(40nm)/Al |  |  |  |  |
| Polymer poly(NVK-co-[Tb(QCHEt2)3(L)]) 50:1 |  | ITO/PEDOT:PSS (30nm)/Polymer (40 nm)/BCP (10 nm)/TPBI (30 nm)/LiF (1 nm)/Al (100 nm) | Green (545, 490, 600) | 81 (16V) Turn on 11V |  | [70] 2017 |
|  |  | ITO/PEDOT:PSS (30 nm)/Polymer (40 nm)/BCP (20 nm)/TPBI (30 nm)/LiF (1 nm)/Al (100 nm) |  | 105 (17) Turn on 11V |  |  |
| [Tb(QiPr)3(TPPO)2] |  | ITO/TPD(40nm)/Complex(40nm)/ALQ( 40nm)/Al | Green (545, 490, 600 nm (Tb) + 410 (TPD Fluorescence) | (15-16V) |  | [54] 1998 |
|  |  | ITO/TPD(20nm)/Complex(20nm)/ALQ( 20nm)/Al |  | (8-12 V)b) |  |  |
|  |  | ITO/TPD(20nm)/Complex(50nm)/ALQ( 50nm)/Al |  | (14-20V) b) |  |  |
|  |  | ITO/TPD(80nm)/Complex(20nm)/ALQ( 20nm)/Al |  | (10-20V) b) |  |  |
|  |  | ITO/TPD(40nm)/Complex(80nm)/Al |  | (12-22V) b) |  |  |
|  |  | ITO/TPD(20nm)/Complex(40nm)/Al |  | (6-20V) b) |  |  |
| [Tb(QtBu)3(TPPO)] |  | ITO/Complex(85 nm)/Mg:Al | Green (490, 545 nm) | 6 (23V) Turn on 17V |  | [63] 2000 |
|  |  | ITO/TPD/Complex/Mg:Al |  | 0.25 (15V) Turn on <10V |  |  |
|  |  | ITO/Complex/AlQ/Mg:Al |  | 12(14V) Turn on 8.5V |  |  |
|  |  | ITO/TPD(40 nm)/Complex (24nm)/TAZ (60 nm)/Mg:Al |  | 9 (14V) 75 (18V) |  |  |
|  |  | ITO/MTDATA (7.5 nm)/TPD (40 nm)/Complex (34 nm)/TAZ/ (60 nm)/Mg:Al |  | 70 (16V) 120 (17V) |  |  |
|  |  | ITO/MTDATA (7.5 nm)/TPD (40 nm)/Complex (34 nm)/TAZ/ (75 nm)/Mg:Al |  | 25 (14V) |  |  |
| [Tb(QtBu)3(TPPO)] |  | ITO/TPD 40 nm / Complex 34 nm /TAZ 55 nm /Mg:Al 10:1) | Green (490, 545 nm) Green Green Green | 130 (22V) Turn on 8V | 3.6 mA/cm2 | [182] 2000 |
|  |  | ITO/TPD 40 nm / Complex 34 nm /TAZ 55 nm /C 5 nm /Al |  | 100 (33V) Turn on 13V |  |  |
|  |  | ITO/TPD 40 nm / Complex 34 nm /TAZ 55 nm /Mg 2 nm /C 20 nm /Al |  | 68 (22V) Turn on 8V | 3.6 mA/cm2 |  |
| [Tb(QtBu)3(TPPO)] |  | ITO/Complex (90 nm)/Ca/Al (100 nm) |  | 226 (17V) | 52 mA/cm2 | [179] 2001 |
|  |  | ITO/Complex (90 nm)/Mg/Al(100 nm) |  |  |  |  |
| [Tb(QiPr)3(phen)] |  | ITO/TPD(15 nm)/ Complex (80 nm)/ Mg0.9Ag0.1 | Pale green (402, 490, 540, 545 nm) | 270 (19V) |  | [55] 2002 |
|  |  | ITO/TPD(5 nm)/ Complex (80 nm)/ Mg0.9Ag0.1 | Yellow (490, 540, 545 nm) | 130 (16V) |  |  |
|  |  | ITO/TPD(20 nm)/ Complex (80 nm)/BCP(20 nm)/ Mg0.9Ag0.1 | Pure green (490, 545 nm) | 250 (15V) Turn on 3V |  |  |
|  |  | ITO/TPD(20 nm)/TPD : Complex (1 : 2)(50 nm)/ Complex /AlQ(30 nm)/Mg0.9Ag0.1 | Yellow (540, 545 nm) | 1180 (17V) |  |  |
| [Tb(QCHEt2)3(TPPO)] |  | ITO/ Complex (80 nm)/ Mg0.9Ag0.1 (200 nm)/Ag (80 nm) | Green (490, 545 nm) | 46 (17V) Turn on 11V |  | [71] 2003 |
|  |  | ITO/TPD (20 nm)/ Complex (50 nm)/AlQ (30 nm)/ Mg0.9Ag0.1 (200 nm)/Ag (80 nm) |  | 20000 (20V) Turn on 4V |  |  |
|  |  | ITO/TPD (20 nm)/ Complex (50 nm)/BCP (20 nm)/AlQ (30 nm)/ Mg0.9Ag0.1 (200 nm)/Ag (80 nm) |  | 8800 (18V) |  |  |
|  |  | ITO/NPB (10 nm)/ Complex (50 nm)/BCP (20 nm)/AlQ (40 nm)/ Mg0.9Ag0.1 (200 nm)/Ag (80 nm) |  | 12000 (18V) |  |  |
| [Tb(QiPr)3(TPPO)2] |  | ITO/ Complex (80 nm)/ Mg0.9Ag0.1 (200 nm)/Ag (80 nm)) | Green (490, 545 nm) | 12 Turn on 11V |  | [56] 2003 |
|  |  | ITO/TPD(20 nm)- Complex (50 nm)-AlQ(30 nm)/ Mg0.9Ag0.1 (200 nm)/Ag (80 nm) |  | 2100 (13V) Turn on 4V | 1.49 lm/W at at 7 V |  |
|  |  | ITO/TPD(20 nm)- Complex (50 nm)-BCP(20 nm)-AlQ(30 nm)/ Mg0.9Ag0.1 (200 nm)/Ag (80 nm) |  | 3100 (14V) | 3.62 lm/W at 6 V |  |
|  |  | ITO/TPD(20 nm)-[TbQiPr3(EtOH)(H2O)] (40 nm)- Complex (30 nm)-AlQ(20 nm)/ Mg0.9Ag0.1 (200 nm)/Ag (80 nm) |  | 2400 (13V) | 0.77 lm/W at 9 V |  |
|  |  | ITO/TPD(20 nm)- Complex (20 nm)- Complex (50 nm)-AlQ(30 nm)/ Mg0.9Ag0.1 (200 nm)/Ag (80 nm) |  | 9600 (15V) | 5.2 lm/W at 9 V |  |
| [Tb(QiPr)3(EtOH)(H2O)] |  | ITO/ Complex (80 nm)/ Mg0.9Ag0.1 (200 nm)/Ag (80 nm) |  | 8.3 Turn on 11V |  |  |
|  |  | ITO/TPD(20 nm)- Complex (50 nm)-AlQ(30 nm)/ Mg0.9Ag0.1 (200 nm)/Ag (80 nm) |  | 18500 (21V) Turn on 4V | 1.11 lm/W at 13 V |  |
|  |  | ITO/TPD(20 nm)- Complex (60 nm)-BCP(20 nm)-AlQ(10 nm)/ Mg0.9Ag0.1 (200 nm)/Ag (80 nm) |  | 2640 (16V) | 0.83 lm/W at 10 V |  |
|  |  | ITO/TPD(40 nm)- Complex (30 nm)-BCP(20 nm)-AlQ(20 nm)/ Mg0.9Ag0.1 (200 nm)/Ag (80 nm) |  | 2800 (12V) | 2.6 lm/W at 6 V |  |
| [Tb(QCHEt2)3(TPPO)] |  | ITO/ Complex (80 nm)/Mg0.9Ag0.1(200 nm)/Ag(80 nm) |  | 46 Turn on 11V |  |  |
|  |  | ITO/TPD(20 nm)- Complex (50 nm)-AlQ(30 nm)/ Mg0.9Ag0.1 (200 nm)/Ag (80 nm) |  | 20000 (20V) Turn on 4V | 3.24 lm/W at 10 V |  |
|  |  | ITO/TPD(20 nm)- Complex (50 nm)-BCP(20 nm)-AlQ(30 nm)/ Mg0.9Ag0.1 (200 nm)/Ag (80 nm) |  | 8800 (18V) | 9.4 lm/W at 7 V |  |
|  |  | ITO/NPB(20 nm)- Complex (50 nm)-BCP(20 nm)-AlQ(30 nm)/ Mg0.9Ag0.1 (200 nm)/Ag (80 nm) |  | 18000 (18V) | 14.0 lm/W at 6 V |  |
|  |  | ITO/NPB(10 nm)- Complex (50 nm)-BCP(20 nm)-AlQ(40 nm)/ Mg0.9Ag0.1 (200 nm)/Ag (80 nm) |  | 12000 (18V) | 11.3 lm/W at 7 V |  |
| [Tb(QiPr)3(DPPOC)] |  | ITO/NPB (30 nm)/co-deposited Complex (20 nm)/BCP (10 nm)/AlQ (30 nm)/ Mg0.9Ag0.1 | Greenish-blue (470 + 490 + 545 nm) |  | 2.6 lm/W at 6.0 V | [57] 2009 |
|  |  | ITO/NPB (30 nm)/co-deposited Complex (30 nm)/BCP (10 nm)/AlQ (30 nm)/ Mg0.9Ag0.1 | Greenish-blue (470 + 490 + 545 nm) | 1331 cd/m2 at 19 V | 5.2 lm/W at 7.0 V |  |
|  |  | ITO/NPB (30 nm)/co-deposited Complex (40 nm)/BCP (10 nm)/AlQ (30 nm)/ Mg0.9Ag0.1 | Green (490 + 545 nm) |  |  |  |
|  |  | ITO/NPB (30 nm)/co-deposited Complex (60 nm)/BCP (10 nm)/AlQ (30 nm)/ Mg0.9Ag0.1 |  | 1020 cd/m2 at 16 V | 5.2 lm/W at 7.0 V |  |
|  |  | ITO/NPB (10 nm)/[TbQiPr3] (10 nm)/ Complex (30 nm)/BCP (10 nm)/AlQ (20 nm)/ Mg0.9Ag0.1 |  |  |  |  |
|  |  | ITO/NPB (10 nm)/ [TbQiPr3] (15 nm)/ Complex (30 nm)/BCP (10 nm)/AlQ (20 nm)/ Mg0.9Ag0.1 |  |  |  |  |
|  |  | ITO/NPB (10 nm)/ [TbQiPr3] (20 nm)/ Complex (30 nm)/BCP (10 nm)/AlQ (20 nm)/ Mg0.9Ag0.1 |  | 2256 cd/m2 at 16 V | 16.1 lm/W at 5 V |  |
| P4 |  | ITO/Polymer (50 nm)/BATH(30 nm)/AlQ(30 nm)/Yb(150 nm) | Green (490 + 545 nm) | 28 cd/m^2 (20.5V) | 0.03 lm/W (20.5 V) | [58] 2012 |
| P5 |  | ITO/ Polymer (50 nm)/BATH(30 nm)/AlQ(30 nm)/Yb(150 nm) |  | 29 cd/m^2 (18.5V) | 0.05 lm/W (18.5 V) |  |
| P6 |  | ITO/ Polymer (50 nm)/BATH(30 nm)/AlQ(30 nm)/Yb(150 nm) |  | 100 cd/m^2 (19.5V) | 0.51 lm/W (12.5 V) |  |
| P1 |  | ITO/ Polymer (40 nm)/BATH(30 nm)/ AlQ (30 nm)/Yb |  | 70 (17.5V) Turn on 8.5 | 0.16 lm/W (11V) | [82] 2014 |
| P2 |  | ITO/ Polymer (40 nm)/BATH(30 nm)/ AlQ (30 nm)/Yb |  | 4 (18.5V) Turn on 14 | 0.0005 (17.5V) |  |
| [Tb(QiPr)3] |  | ITO/ MoO3 (1 nm)/NPB (35 nm)/ Complex: DPPOC (1 : 1) (20 nm)/Alq3 (40 nm)/LiF (1 nm)/Al (100 nm) | Green (490 + 545 nm) | 3823 (7.9V) | 5.0 lm/W | [180] 2015 |
|  |  | ITO/ MoO3 (1 nm)/TCTA (35 nm)/ Complex:DPPOC (1:1) (20 nm)/TPBi (40 nm)/LiF (1 nm)/Al (100 nm) |  | 2592 (5.3V) | 25 lm/W |  |
|  |  | ITO/ MoO3 (1 nm)/TCTA (35 nm)/ Complex:DPPOC (1:1) (20 nm)/3TPYMB (40 nm)/LiF (1 nm)/Al (100 nm) |  | 1672 (6.6V) | 35 lm/W |  |
|  |  | ITO/ MoO3 (1 nm)/TCTA (35 nm)/ Complex 3:DCPPO (1:1) (10 nm)/ Complex:DPPOC (1:1) (10 nm)/3TPYMB (40 nm)/LiF (1 nm)/Al (100 nm) |  | 2438 (6.4V) | 34 lm/W |  |
|  |  | ITO/MoO3 (1 nm)/TCTA: MoO3 (20%) (20 nm)/TCTA (15 nm)/ Complex:DCPPO (1:1) (10 nm)/ Complex:DPPOC (1:1) (10 nm)/3TPYMB (50 nm)/LiF (1 nm)/Al (100 nm) |  | 2784 (4.6V) | 52 lm/W |  |
| [Tb(QPhCF3Me)3(TDZP)] |  | ITO/PEDOT:PSS (25 nm)/TCTA:OXD-7: Complex (20 nm)/Tm3PyPB (50 nm)/LiF (1 nm)/Al (100 nm) | Green (490 + 545 nm) | 512.78 Turn on 3.1 V | 6.56 lm/W | [116] 2018 |
|  |  | ITO/PEDOT:PSS (25 nm)/TCTA:OXD-7: Complex (20 nm)/Tm3PyPB (50 nm)/LiF (1 nm)/Al (100 nm) |  | 6364.98 Turn on 2.3 V | 12.38 lm/W |  |
|  |  | ITO/PEDOT:PSS (25 nm)/TCTA:OXD-7: Complex (20 nm)/Tm3PyPB (50 nm)/LiF (1 nm)/Al (100 nm) |  | 1269.14 Turn on 2.9 V | 4.79 lm/W |  |
|  |  | ITO/PEDOT:PSS (25 nm)/TCTA:OXD-7: Complex (20 nm)/Tm3PyPB (50 nm)/LiF (1 nm)/Al (100 nm) |  | 5997.96 Turn on 2.40 V | 11.55 lm/W |  |
| [Tb(QiPr)3(TPPO)2] |  | ITO/TPD(42 nm)/Complex (42 nm)/ /AlQ(42nm)/Al (50 nm) | Green (545 + 490) nm | 920 (18V) | 0.51 lm/W | [60] 1998 |
|  |  | ITO/TPD(40 nm)/Complex (64 nm)/ Al (50 nm) | Greenish blue (405+545+490)nm |  |  |  |
| Dy-based OLEDs |  |  |  |  |  |  |
| [Dy(QiPr)3(TPPO)2] |  | ITO/Complex (80 nm)/ LiF (1 nm)/Al (100 nm) | No emission |  |  | [50] 2007 |
|  |  | ITO/ TPD (50 nm)/Complex (50 nm)/LiF (1 nm)/Al (100 nm) | White 410 nm, 572 nm, 480 nm | 98(11.9) |  |  |
|  |  | ITO/ Complex(50 nm)/AlQ (20 nm)/LiF (1 nm)/ Al (100 nm) | Yellow 572 nm, 480 nm | n/a |  |  |
|  |  | ITO/TPD (50 nm)/ Complex(50 nm)/AlQ (20 nm) /LiF (1 nm) /Al (100 nm) | White 520+572 nm | n/a |  |  |
|  |  | ITO/TPD (20 nm)/ Complex (50 nm)/BCP (20 nm)/ AlQ (30 nm)/LiF (1 nm)/Al (100 nm) | White 500+572 nm, 480 nm | 424 |  |  |
|  |  | ITO/CuPc (15 nm)/ Complex(50 nm)/BCP (20 nm)/AlQ (30 nm)/LiF (1 nm)/Al (100 nm) | Yellow (480+572 nm) | 277(19) |  |  |
|  |  | ITO/CuPc (15 nm)/ Complex(70 nm)/BCP (20 nm)/AlQ (30 nm)/LiF (1 nm)/Al (100 nm) | Yellow (480+572 nm) | 524(19) |  |  |
| Er-based OLEDs |  |  |  |  |  |  |
| [Er(QiPr)3(TPPO)2] |  | ITO/ NPB 40 nm/ Complex 60 nm/LiF 1 nm/Al 120 nm | NIR (1538 nm) | 123(21) |  | [51] 2008 |
|  |  | ITO/NPB 20 nm/ Complex 50 nm/AlQ 40 nm/LiF 1 nm/ Al 120 nm. |  | 254(19) |  |  |
|  |  | ITO/NPB 20 nm/ Complex 50 nm/BCP 20 nm/AlQ 40 nm/LiF 1 nm/Al 120 nm |  | 224(19) |  |  |
| Yb-based OLEDs |  |  |  |  |  |  |
| [Yb(QiPr)3(bath)] (complex 1) [Yb(QiPr)3(TPPO)2] (complex 2) |  | ITO/NPB(20 nm)/ (complex 1) (50 nm)/AlQ(40 nm)/LiF/Al(150 nm) | NIR (980 nm, Yb) + 451 nm (NPB) |  | 1.4 mW/m2 (14.6V) | [43] 2012 |
|  |  | ITO/NPB(nm)/NPB+(complex 1) (30 nm)/ (complex 1) (55 nm)/LiF/Al(150 nm) | NIR (980 nm, Yb) + 451 nm (NPB) | Turn on 6.3V | 4.2 mW/m2 (6.3V) |  |
|  |  | ITO/NPB(30 nm)/ (complex 2) (50 nm)/BCP(20 nm)/Alq3(30 nm)/LiF/Al(150 nm) | NIR (980 nm, Yb) + 470 nm BCP) | Turn on 10V | 8.0 mW/m2 (6.3V) |  |
|  |  | ITO/NPB(20 nm)/(complex 2) (20 nm)/ (complex 1)(40 nm)/BCP(20 nm)/Alq3(30 nm)/LiF(1 nm)/Al(150 nm) | NIR (980 nm, Yb) | Turn on 6.7V | 14.7 mW/m2 (6.3V) |  |
| [Yb(QCF3)3(bipy)] |  | ITO/ MoO3 (1 nm)/ NPB (40 nm) /Bebq2: Complex (20 nm)/Bebq2 (40 nm)/LiF (1.2 nm)/ Al | IR, (978+1006+1034, Yb) | (15V) Turn on 5.5V | 1.83 (978 nm) 1.63 (1005 nm) | [90] 2022 |
| [Yb(QCF3)3(phen)] |  | ITO/ MoO3 (1 nm)/ NPB (40 nm) /Bebq2: Complex (20 nm)/Bebq2 (40 nm)/LiF (1.2 nm)/ Al | IR, (978+1005+1034, Yb) | (16 V) Turn on 5.5V | 2.04 (978 nm) 1.84 (1005 nm) |  |
| [Yb(QCF3)3(bath)] |  | ITO/ MoO3 (1 nm)/ NPB (40 nm) /Bebq2: Complex (20 nm)/Bebq2 (40 nm)/LiF (1.2 nm)/ Al | IR, (978+1005+1031 nm, Yb) | (14 V) Turn on 5V | 2.17 (978 nm) 1.92 (1005 nm) |  |
| Lu-based OLEDs |  |  |  |  |  |  |
| [Lu(QiPr)3(TPPO)2] |  | ITO/TPD(40 nm)/ Complex (40 nm)/Mg0.9Ag0.1 | Blue (403nm) |  |  | [49] 2003 |
|  |  | ITO/TPD(40 nm)/ Complex (40 nm)/AlQ(40 nm)/ Mg0.9Ag0.1 | Blue-green (513) |  |  |  |
|  |  | ITO/TPD(20 nm)/ Complex (40 nm)/BCP(20 nm)/AlQ(40 nm)/ Mg0.9Ag0.1 | Blue (465nm) | 119(19V) |  |  |
| [Lu(QiPr)3(bipy)] |  | ITO/TPD(40 nm)/ Complex (40 nm)/ Mg0.9Ag0.1 | Blue-green (513) | 160(19V) |  |  |
|  |  | ITO/TPD(20 nm)/ Complex (60 nm)/ Mg0.9Ag0.1 |  |  |  |  |
|  |  | ITO/ TPD(10 nm)/ Complex (50 nm)/BCP(20 nm)/AlQ(40 nm)/ Mg0.9Ag0.1 |  | 1010 (16V) Turn on 3V |  |  |
| [Lu(QiPr)3(phen)] |  | ITO/TPD(15 nm)/ Complex (95 nm)/ Mg0.9Ag0.1 |  | 475 (17V) |  |  |
|  |  | ITO/TPD(5 nm)/ Complex (40 nm)/BCP (20 nm)/ AlQ(40 nm)/ Mg0.9Ag0.1 |  | 776(17 V) |  |  |

a) AlQ = tris(8-hydroxy- quinolinato)aluminum; BATH = 4,7-Diphenyl-1,10- phenanthroline; BCP = 2,9-dimethyl-4,7- diphenyl-1,10-phenyanthroline; Bebq2 = bis(10-hydroxybenzo[h]quinolinato)beryllium; CBP = 4,4′-bis(arbazole-9- yl)biphenyl; CBS = 4,4’ -bis(2,2-di(2-methoxyphenyl)ethenyl)-1, 1’ -biphenyl; CuPc = Copper phthalocyanine; NPB = N,N′-diphenyl-N,N′-bis(1-naph- thyl)-1,1′-diphenyl-4,4′-diamine; OXD-7 (1,3-bis[2-(4- tert butylphenyl)-1,3,4-oxadiazo-5-yl]benzene); PEDOT = poly(3,4- ethylenedioxythiophene; Poly-TPD (Poly(N,N-bis-4-butylphenyl-N,N-bisphenyl)benzidine); PSS = poly(styrenesulfonate); PVK = (poly(N-vinylcarbazole); TaTC = (Tris(4-carbazoyl-9-ylphenyl)amine); Tm3PyPB = (1,3,5-Tri(m-pyridin-3-ylphenyl)benzene); TPBi =1, 3, 5-tris(2-N-phenylbenzimidazolyl); TPD = N,N’ -bis(3- methylphenyl)-N,N’ -diphenyl-benzidine

Legenda:

Conclusions

Two surges of interest in acylpyrazolone - lanthanide systems associated with extraction separation in the 1960s and 1970s and their use in OLED devices at the turn of the 20th and 21st centuries have had a significant impact on the development of the entire coordination chemistry of rare earth elements. To date, the number of described crystal structures of compounds of this type according to the Cambridge Structural Data Bank (CCDC) exceeds 100, and the number of articles and patents according to SciFinder exceeds 300. This array of information requires understanding and systematization, which we have tried to provide in this review. The main conclusions that we believe it is necessary to make are as follows:

1. To create luminescent materials, the design of ligands should include a competent account of the energy of triplet levels. Systematic study of the dependence of the triplet level energy on the nature of the substituents, especially in the R1 and R2 positions, will allow the creation of new compounds that effectively sensitize the luminescence of IR-emitting ions. It is also interesting to construct correlations between the triplet level energies and the structure of the ligands at a deeper level than truisms such as “an aromatic substituent should lower T”.

2. Tetrakis-anions [LnQ4]- are a convenient alternative to heteroligand complexes, since they also effectively suppress quenching on OH-bond vibrations of solvent molecules and can be used if the ionic nature of the complex does not interfere with technological processes in the device. Otherwise, for example, when creating OLED, a rational choice is phosphine oxide additional ligands, leading to the formation of complexes of the [LnQ3(L)1-2] type.

3. LMCT quenching characteristic of Eu3+ complexes is an obvious obstacle to the use of acylpyrazolonates of this metal, but the ability to control it, for example, by replacing the outer-sphere cation or, possibly, changing the ligand structure makes it possible to create turn-on systems, which opens up prospects for the creation of sensor materials.

4. Bisacylpyrazolonates have been significantly less studied than derivatives of simple HQ proligands, and this seems to be a big omission. Binuclear systems will allow us to implement and study subtle effects associated with magnetic processes, excitation energy transfer and luminescence. The transition to more complex multinuclear systems also seems promising, and the stumbling block - the difficulty of obtaining single crystals suitable for X-ray structural analysis - can be eliminated with careful selection of a solvent and a solvothermal synthesis method.

5. Only a few works use the fundamental difference between acylpyrazolones and traditional diketones - the presence of additional donor nitrogen atoms. This difference makes it possible to create d-f heterometallic complexes, which are extremely interesting and can give the world new amazing materials. This direction also seems to us to be extremely important and can potentially act as a trigger for the third period of growth of interest in acylpyrazolonates of rare earth elements.

6. Compared to derivatives of other ligands, acylpyrazolonates of lanthanides remain terra incognita from the point of view of studying magnetic properties. This currently most important topic is practically ignored in the cited articles, which also seems to be a significant omission and awaits its researcher.

Acknowledgements

This work was supported by the Russian Science Foundation under the project 23-23-00393 and by Fondazione NEST (Network 4 Energy Sustainable Transition funded by NextGenerationEU, Mission 4, Component 2). University of Camerino and MUR are also acknowledged for a grant to Alessia Tombesi.

References

[1]	B.S. Jensen, H. Meier, K. Lundquist, S. Refn, The Synthesis of 1-Phenyl-3-methyl-4-acyl-pyrazolones-5., Acta Chem. Scand. 13 (1959) 1668–1670. https://doi.org/10.3891/acta.chem.scand.13-1668.

[2]	B.S. Jensen, N.A. Sörensen, C.E. Jensen, Solvent Extraction of Metal Chelates. II. An Investigation of some 1-Phenyl-3-methyl-4-acyl-pyrazolones-5., Acta Chem. Scand. 13 (1959) 1890–1896. https://doi.org/10.3891/acta.chem.scand.13-1890.

[3]	I.P. Efimov, L.S. Voronets, V.M. Peshkova, Reaction of cerium with 1-phenyl-3-methyl-4-thienoyl-5-pyrazolone, Vestn. Mosk. Univ. Seriya 2 Khimiya. 11 (1970) 490–491.

[4]	I.P. Efimov, L.G. Tomilova, L.S. Voronets, V.M. Peshkova, Reaction of some rare earth elements with 1-phenyl-3-methyl-4-benzoyl-5-pyrazolone, Zhurnal Anal. Khimii. 28 (1973) 267–271.

[5]	N.M. Kuzmin, Y.A. Zolotov, Ekstraktsiya Metallov Atsilpirazolonami (Extraction of Metals by Acylpyrazolones), Nauka, Moscow, 1977.

[6]	K. Sasayama, S. Umetani, M. Matsui, The substitent effect on the synergic extraction of europium and scandium with 1-phenyl-3-methyl-4-acylpyrazol-5-one and tri and tri-n-octylphosphine oxide, Anal. Chim. Acta. 149 (1983) 253–258. https://doi.org/10.1016/S0003-2670(00)83181-5.

[7]	Q. Jia, Q. Shang, W. Zhou, Synergistic extraction of lanthanum(III) from a nitrate medium by mixtures of 1-phenyl-3-methyl-4-benzoyl-pyrazalone-5 and triisobutylphosphine sulfide, Ind. Eng. Chem. Res. 43 (2004) 6703–6707. https://doi.org/10.1021/ie049831u.

[8]	S. Varbanov, E. Tashev, N. Vassilev, M. Atanassova, V. Lachkova, T. Tosheva, S. Shenkov, I. Dukov, Hexa(1,1,3,3-tetramethyl-butyl)-hexakis(dimethylphosphinoyl-methoxy)-calix[6]arene: Synthesis, characterization and implementation as a synergistic agent in the solvent extraction of lanthanoids, Polyhedron. 134 (2017) 135–142. https://doi.org/10.1016/j.poly.2017.06.013.

[9]	S.I. Weissman, Intramolecular Energy Transfer The Fluorescence of Complexes of Europium, J. Chem. Phys. 10 (1942) 214–217. https://doi.org/10.1063/1.1723709.

[10]	J.-C.G. Bünzli, C. Piguet, Taking advantage of luminescent lanthanide ions, Chem. Soc. Rev. 34 (2005) 1048. https://doi.org/10.1039/b406082m.

[11]	J.-C.G. Bünzli, S. V. Eliseeva, Basics of Lanthanide Photophysics, in: 2010: pp. 1–45. https://doi.org/10.1007/4243_2010_3.

[12]	S. Sato, M. Wada, Relations between Intramolecular Energy Transfer Efficiencies and Triplet State Energies in Rare Earth β-diketone Chelates, Bull. Chem. Soc. Jpn. 43 (1970) 1955–1962. https://doi.org/10.1246/bcsj.43.1955.

[13]	G.A. Crosby, R.E. Whan, J.J. Freeman, Spectroscopic studies of rare earth chelates, J. Phys. Chem. 66 (1962) 2493–2499. https://doi.org/10.1021/j100818a041.

[14]	E.T. Karaseva, V.E. Karasev, Effect of phosphine oxides on the luminescent properties of rare earth element complexes with 1- phenyl-3-methyl-4-benzoylpyrazol-5-one, Russ. J. Coord. Chem. Khimiya. 1 (1975) 926–929.

[15]	E.T. Karaseva, V.E. Karasev, N.I. Sigula, A.P. Golovina, I.P. Efimov, Sintez i fiziko-khimicheskiye svoystva raznoligandnykh kompleksov RZE s 1-fenil-3-metil-4-benzoilpirazolonom-5 i triizobutilfosfatom // Synthesis and physicochemical properties of mixed-ligand rare earth complexes with 1-phenyl-3-methyl-4-benzoylpyrazolon, Russ. J. Coord. Chem. Khimiya. 5 (1979) 647–652.

[16]	C.X. Zhao, Y.J. Ding, T.T. Yuan, D.Y. Wanyan, Y.J. Guo, Z.Z. Hu, X. Li, Syntheses and Crystal Structure of Ce (IV) Complex Containing 4-Heterocyclic Acylpyrazolone, Asian J. Chem. 26 (2014) 8604.

[17]	F. Marchetti, C. Pettinari, R. Pettinari, Acylpyrazolone ligands : Synthesis , structures , metal coordination chemistry and applications, Coord. Chem. Rev. 249 (2005) 2909–2945. https://doi.org/10.1016/j.ccr.2005.03.013.

[18]	Y.A. Belousov, A.A. Drozdov, Lanthanide acylpyrazolonates: synthesis, properties and structural features, Russ. Chem. Rev. 81 (2012) 1159–1169. https://doi.org/10.1070/rc2012v081n12abeh004255.

[19]	A.O. Zoss, G.F. Hennion, Preparation, Properties and Derivatives of α-Acetylenic Acids 1, J. Am. Chem. Soc. 63 (1941) 1151–1153. https://doi.org/10.1021/ja01849a077.

[20]	K. TABEI, E. KAWASHIMA, T. KATO, Reaction of N-hydroxyacetoacetanilide with carbonyl reagents., Chem. Pharm. Bull. 29 (1981) 244–249. https://doi.org/10.1248/cpb.29.244.

[21]	Y.-F. Zhu, B.-L. Wei, J.-J. Wei, W.-Q. Wang, W.-B. Song, L.-J. Xuan, Synthesis of pyrazolones and pyrazoles via Pd-catalyzed aerobic oxidative dehydrogenation, Tetrahedron Lett. 60 (2019) 1202–1205. https://doi.org/10.1016/j.tetlet.2019.03.063.

[22]	Y.-Y. Huang, H.-C. Lin, K.-M. Cheng, W.-N. Su, K.-C. Sung, T.-P. Lin, J.-J. Huang, S.-K. Lin, F.F. Wong, Efficient di-bromination of 5-pyrazolones and 5-hydroxypyrazoles by N-bromobenzamide, Tetrahedron. 65 (2009) 9592–9597. https://doi.org/10.1016/j.tet.2009.09.055.

[23]	K. Cheng, J. Bin Wu, H. Lin, J. Huang, Y. Huang, S. Lin, T. Lin, F.F. Wong, Dibromination of 5‐pyrazolones and 5‐hydroxypyrazoles via dibromoisocyanuric acid, J. Heterocycl. Chem. 47 (2010) 1153–1156. https://doi.org/10.1002/jhet.442.

[24]	N. Desroy, F. Moreau, S. Briet, G. Le Fralliec, S. Floquet, L. Durant, V. Vongsouthi, V. Gerusz, A. Denis, S. Escaich, Towards Gram-negative antivirulence drugs: New inhibitors of HldE kinase, Bioorg. Med. Chem. 17 (2009) 1276–1289. https://doi.org/10.1016/j.bmc.2008.12.021.

[25]	T. Yoshizumi, H. Miyazoe, H. Ito, T. Tsujita, H. Takahashi, M. Asai, S. Ozaki, H. Ohta, O. Okamoto, Design, synthesis, and structure–activity relationship study of a novel class of ORL1 receptor antagonists based on N-biarylmethyl spiropiperidine, Bioorg. Med. Chem. Lett. 18 (2008) 3778–3782. https://doi.org/10.1016/j.bmcl.2008.05.036.

[26]	M.S.K. Youssef, S.A.M. Metwally, M.A. El‐Maghraby, M.I. Younes, Synthesis of pyrazolo[4,3‐ d ]oxazoles, J. Heterocycl. Chem. 21 (1984) 1747–1752. https://doi.org/10.1002/jhet.5570210635.

[27]	T.I. Kolodyazhna, D.A. Lega, S.Y. Suikov, A.A. Kyrylchuk, M. V. Vovk, V.P. Chernykh, L.A. Shemchuk, Some Aspects of 4H-Pyrans Synthesis Based on 4-Chloro-1-ethyl-1H-benzo[c][1,2]thiazine-3-carbaldehyde 2,2-dioxide: Antimicrobial Activity of the Compounds Synthesized, ChemistrySelect. 6 (2021) 14005–14012. https://doi.org/10.1002/slct.202104103.

[28]	T. Chandra, N. Garg, S. Lata, K.K. Saxena, A. Kumar, Synthesis of substituted acridinyl pyrazoline derivatives and their evaluation for anti-inflammatory activity, Eur. J. Med. Chem. 45 (2010) 1772–1776. https://doi.org/10.1016/j.ejmech.2010.01.009.

[29]	L.F. Tietze, A. Steinmetz, A General and Expedient Method for the Solid-Phase Synthesis of Structurally Diverse 1-Phenylpyrazolone Derivatives, Synlett. 1996 (1996) 667–668. https://doi.org/10.1055/s-1996-5548.

[30]	L. Shen, M. Shi, F. Li, D. Zhang, X. Li, E. Shi, T. Yi, Y. Du, C. Huang, Polyaryl ether dendrimer with a 4-phenylacetyl-5-pyrazolone-based terbium(III) complex as core: Synthesis and photopysical properties, Inorg. Chem. 45 (2006) 6188–6197. https://doi.org/10.1021/ic052148v.

[31]	J.-N. Tan, M. Li, Y. Gu, Multicomponent reactions of 1,3-disubstituted 5-pyrazolones and formaldehyde in environmentally benign solvent systems and their variations with more fundamental substrates, Green Chem. 12 (2010) 908. https://doi.org/10.1039/b924699a.

[32]	A. V. Safronova, L.N. Bochkarev, E. V. Baranov, Synthesis, structure, and some properties of 1-phenyl-3-methyl-4-(2,3,4,5,6-pentafluorobenzoyl)pyrazol-5-one and its lanthanide complexes, Russ. J. Coord. Chem. Khimiya. 41 (2015) 118–128. https://doi.org/10.1134/S1070328415010091.

[33]	Y.A. Belousov, V.M. Korshunov, M.T. Metlin, D.A. Metlina, M.A. Kiskin, D.F. Aminev, N.P. Datskevich, A.A. Drozdov, C. Pettinari, F. Marchetti, I. V. Taydakov, Towards bright dysprosium emitters: Single and combined effects of environmental symmetry, deuteration, and gadolinium dilution, Dye. Pigment. 199 (2022) 110078. https://doi.org/10.1016/j.dyepig.2021.110078.

[34]	V.F. Shul’Gin, O. V. Konnik, S. V. Abkhairova, A.N. Gusev, S.B. Meshkova, A. V. Kiriyak, E.B. Rusanov, M. Hasegawa, W. Linert, Anionic lanthanide complexes with 3-methyl-1-phenyl-4-formylpyrazole-5-one and hydroxonium as counter ion, Inorganica Chim. Acta. 402 (2013) 33–38. https://doi.org/10.1016/j.ica.2013.03.044.

[35]	O. V. Konnik, V.F. Shul’Gin, S. V. Abkhairova, S.B. Meshkova, E.B. Rusanov, V. V. Minin, Heteroligand complexes of lanthanides with 4-formyl-3-methyl-1- phenylpyrazol-5-one and 1,10-phenanthroline, Russ. J. Coord. Chem. Khimiya. 40 (2014) 28–33. https://doi.org/10.1134/S1070328414010035.

[36]	V.F. Shul’Gin, S. V. Abkhairova, O. V. Konnik, S.B. Meshkova, Z.M. Topilova, E.B. Rusanov, G.G. Aleksandrov, I.L. Eremenko, Anionic lanthanide complexes with 3-methyl-4-formyl-1-phenyl-5-pyrazolone, Russ. J. Inorg. Chem. 58 (2013) 678–683. https://doi.org/10.1134/S0036023613060223.

[37]	V. Shul’gin, N. Pevzner, A. Gusev, M. Sokolov, V. Panyushkin, J. Devterova, K. Kirillov, I. Martynenko, W. Linert, Tb(III) complexes with 1-phenyl-3-methyl-4-stearoyl-pyrazol-5-one as a material for luminescence Langmuir–Blodgett films, J. Coord. Chem. 71 (2018) 4228–4236. https://doi.org/10.1080/00958972.2018.1536783.

[38]	X.L. Li, J. Li, C. Zhu, B. Han, Y. Liu, Z. Yin, F. Li, C.M. Liu, An intense luminescent Dy(iii) single-ion magnet with the acylpyrazolonate ligand showing two slow magnetic relaxation processes, New J. Chem. 42 (2018) 16992–16998. https://doi.org/10.1039/c8nj03345e.

[39]	D. Zhou, Q. Li, C. Huang, G. Yao, S. Umetani, M. Matsui, L. Ying, A. Yu, X. Zhao, Room-temperature fluorescence, phosphorescence and crystal structure of 4-acyl pyrazolone lanthanide complexes: Ln(L)3·2H2O, Polyhedron. 16 (1997) 1381–1389. https://doi.org/10.1016/s0277-5387(96)00382-8.

[40]	X.C. Gao, H. Cao, C.H. Huang, S. Umitani, G.Q. Chen, P. Jiang, Photoluminescence and electroluminescence of a series of terbium complexes, Synth. Met. 99 (1999) 127–132. https://doi.org/10.1016/s0379-6779(98)01487-8.

[41]	D. Zhang, M. Shi, Z. Liu, F. Li, T. Yi, C. Huang, Luminescence modulation of a terbium complex with anions and its application as a reagent, Eur. J. Inorg. Chem. 3 (2006) 2277–2284. https://doi.org/10.1002/ejic.200501064.

[42]	Z. Li, J. Yu, L. Zhou, H. Zhang, R. Deng, The optical properties and the natural lifetime calculation of a Sm(III) complex, Inorg. Chem. Commun. 11 (2008) 1284–1287. https://doi.org/10.1016/j.inoche.2008.08.008.

[43]	Z. Li, H. Zhang, J. Yu, Near-infrared electroluminescence from double-emission-layers devices based on Ytterbium (III) complexes, Thin Solid Films. 520 (2012) 3663–3667. https://doi.org/10.1016/j.tsf.2011.12.052.

[44]	Z. Li, J. Yu, The near-infrared optical properties and Judd-Ofelt analysis of a Dy(III) complex, J. Lumin. 143 (2013) 169–172. https://doi.org/10.1016/j.jlumin.2013.04.044.

[45]	Q.Y. Cao, L.Q. Huang, Z.W. Wang, C.J. Yang, X.C. Cao, Tris[4-(3-methyl-4-oxo-1-phenyl-4,5-dihydro-1 Hpyrazol-4-ylidene) isobutanolato-κ2O,O′]bis(triphenylphosphine oxide-κO)europium(III), Acta Crystallogr. Sect. E Struct. Reports Online. 61 (2005). https://doi.org/10.1107/S160053680503446X.

[46]	A. V. Safronova, L.N. Bochkarev, I.P. Malysheva, E. V. Baranov, Facile synthesis of rare-earth pyrazolonates by the reaction of rare-earth metals with 1-phenyl-3-methyl-4-isobutyryl-5-pyrazolone. Crystal structures of [Ln(PMIP)3]2 (Ln=Y, Gd, Tb, Er, Tm), Inorganica Chim. Acta. 392 (2012) 454–458. https://doi.org/10.1016/j.ica.2012.03.032.

[47]	M. Shi, F. Li, T. Yi, D. Zhang, H. Hu, C. Huang, Tuning the Triplet Energy Levels of Pyrazolone Ligands to Match the 5 D 0 Level of Europium(III), Inorg. Chem. 44 (2005) 8929–8936. https://doi.org/10.1021/ic050844p.

[48]	L. Huang, H. Tian, F.Y. Li, D.Q. Gao, Y.Y. Huang, C.H. Huang, Blue organic electroluminescent devices based on a distyrylarylene derivative as emitting layer and a terbium complex as electron-transporting layer, J. Lumin. 97 (2002) 55–59. https://doi.org/10.1016/S0022-2313(01)00427-6.

[49]	H. Xin, M. Shi, F.Y. Li, M. Guan, D.Q. Gao, C.H. Huang, K. Ibrahim, F.Q. Liu, Photoluminescence and electroluminescence properties of three ternary lutetium complexes, New J. Chem. 27 (2003) 1485–1489. https://doi.org/10.1039/b304451c.

[50]	Z.F. Li, L. Zhou, J.B. Yu, H.J. Zhang, R.P. Deng, Z.P. Peng, Z.Y. Guo, Synthesis, structure, photoluminescence, and electroluminescence properties of a new dysprosium complex, J. Phys. Chem. C. 111 (2007) 2295–2300. https://doi.org/10.1021/jp064749t.

[51]	Z. Li, J. Yu, L. Zhou, H. Zhang, R. Deng, Z. Guo, 1.54 μm Near-infrared photoluminescent and electroluminescent properties of a new Erbium (III) organic complex, Org. Electron. 9 (2008) 487–494. https://doi.org/10.1016/j.orgel.2008.02.010.

[52]	D.-Q. Gao, C.-H. Huang, K. Ibrahim, F.-Q. Liu, An organic electroluminescent device made from a gadolinium complex, Solid State Commun. 121 (2002) 145–147. https://doi.org/10.1016/S0038-1098(01)00467-7.

[53]	Z. Li, J. Yu, L. Zhou, R. Deng, H. Zhang, The near-infrared optical properties of an Nd (III) complex and its potential application in electroluminescence, Inorg. Chem. Commun. 12 (2009) 151–153. https://doi.org/10.1016/j.inoche.2008.12.001.

[54]	X.C. Gao, H. Cao, C.H. Huang, B.G. Li, K. Ibrahim, F.Q. Liu, S. Umitani, Electroluminescence from both a light-emitting layer and hole transport layer: Spectral evidence for charge carrier tunneling injection, Chem. Phys. Lett. 297 (1998) 530–536. https://doi.org/10.1016/S0009-2614(98)01164-6.

[55]	H. Xin, M. Guang, F.Y. Li, Z.Q. Bian, C.H. Huang, K. Ibrahim, F.Q. Liu, Photoluminescence and electroluminescence of the exciplex formed between a terbium ternary complex and N,N′-diphenyl-N,N′-bis(3-methylphenyl)-1,1′-diphenyl-4,4 ′-diamine, Phys. Chem. Chem. Phys. 4 (2002) 5895–5898. https://doi.org/10.1039/b207990a.

[56]	H. Xin, M. Shi, X.M. Zhang, F.Y. Li, Z.Q. Bian, K. Ibrahim, F.Q. Liu, C.H. Huang, Carrier-transport, photoluminescence, and electroluminescence properties comparison of a series of terbium complexes with different structures, Chem. Mater. 15 (2003) 3728–3733. https://doi.org/10.1021/cm0344414.

[57]	Z. Chen, F. Ding, F. Hao, Z. Bian, B. Ding, Y. Zhu, F. Chen, C. Huang, A highly efficient OLED based on terbium complexes, Org. Electron. 10 (2009) 939–947. https://doi.org/10.1016/j.orgel.2009.04.023.

[58]	A. V. Rozhkov, L.N. Bochkarev, G. V. Basova, I.P. Malysheva, Y.E. Begantsova, E.O. Platonova, E. V. Baranov, Y.A. Kurskii, V.A. Il’Ichev, M.A. Lopatin, G.A. Abakumov, M.N. Bochkarev, Terbium-containing copolymers based on the norbornene functional derivatives. Synthesis, photoluminescent and electroluminescent properties, Russ. J. Gen. Chem. 82 (2012) 1895–1908. https://doi.org/10.1134/S1070363212120018.

[59]	H. Xin, M. Sun, K.Z. Wang, Y.A. Zhang, L.P. Jin, C.H. Huang, Voltage-independent pure red devices based on a carbazole-functionalized europium complex, Chem. Phys. Lett. 388 (2004) 55–57. https://doi.org/10.1016/j.cplett.2004.02.073.

[60]	X.C. Gao, H. Cao, C. Huang, B. Li, S. Umitani, Electroluminescence of a novel terbium complex, Appl. Phys. Lett. 72 (1998) 2217–2219. https://doi.org/10.1063/1.121327.

[61]	L.I.Q.D.C.G.Y.Z. ZHENGHE, Synthesis, characterization and luminescence of Tb(III)-1-phenyl-3-methyl-4-acyl-5-pyrazolone ternary complexes, Acta Chim. Sin. 56 (n.d.) 52–57. https://sioc-journal.cn/Jwk_hxxb.

[62]	A. V. Safronova, L.N. Bochkarev, E. V. Baranov, Synthesis of lanthanide pyrazolonate complexes by the reactions of 1-Phenyl-3-methyl-4-(2,2-dimethylpropan-1-oyl)pyrazol-5-one with metallic lanthanides. Crystal structures of [Ln(Bu t -PMP)3] 2 (Ln = Gd, Tb, and Tm), Russ. J. Coord. Chem. Khimiya. 39 (2013) 537–543. https://doi.org/10.1134/S1070328413060080.

[63]	S. Capecchi, O. Renault, D.-G. Moon, M. Halim, M. Etchells, P.J. Dobson, O. V. Salata, V. Christou, High-Efficiency Organic Electroluminescent Devices Using an Organoterbium Emitter, Adv. Mater. 12 (2000) 1591–1594. https://doi.org/10.1002/1521-4095(200011)12:21<1591::AID-ADMA1591>3.0.CO;2-P.

[64]	J.R.G. Thorne, J.M. Rey, R.G. Denning, S.E. Watkins, M. Etchells, M. Green, V. Christou, Excited state dynamics of organo-lanthanide electroluminescent phosphors: The properties of Tb(tb-pmp)3 and Gd(tb-pmp)3, J. Phys. Chem. A. 106 (2002) 4014–4021. https://doi.org/10.1021/jp013955s.

[65]	H. Xin, M. Shi, X.C. Gao, Y.Y. Huang, Z.L. Gong, D.B. Nie, H. Cao, Z.Q. Bian, F.Y. Li, C.H. Huang, The effect of different neutral ligands on photoluminescence and electroluminescence properties of ternary terbium complexes, J. Phys. Chem. B. 108 (2004) 10796–10800. https://doi.org/10.1021/jp037816h.

[66]	Y. Sun, J. Liu, B. Wang, S. Hou, Y. Zhang, G. Fu, X. Lü, Straightforward and high-performance white-light of an isostructurally organo-(Gd3+x,Tb3+y,Sm3+1-x-y)-ternary blending through typical trichromatic integration, Inorg. Chem. Commun. 145 (2022) 110021. https://doi.org/10.1016/j.inoche.2022.110021.

[67]	J. Liu, W. Li, B. Wang, Y. He, T. Miao, X. Lü, G. Fu, Single-component white polymer light-emitting diode (WPLED) based on a binary tris-pyrazolonate-Sm-complex, J. Lumin. 221 (2020) 117054. https://doi.org/10.1016/j.jlumin.2020.117054.

[68]	Y.A. Belousov, A.A. Drozdov, P.P. Verteletskii, A.A. Prishchenko, L.I. Livantsova, O.P. Novikova, Mixed-ligand lanthanide complexes with acylpyrazolones and phosphorus-containing ligands, Russ. J. Coord. Chem. Khimiya. 39 (2013) 278–282. https://doi.org/10.1134/S1070328413030020.

[69]	D.-J. Qian, W.-N. Leng, Y. Zhang, Z. Chen, J. Van Houten, A study of the fluorescence of some newly synthesized europium complexes with pyrazolone derivatives, Spectrochim. Acta Part A Mol. Biomol. Spectrosc. 56 (2000) 2645–2651. https://doi.org/10.1016/S1386-1425(00)00306-1.

[70]	L. Liu, M. Pang, H. Chen, G. Fu, B. Li, X. Lü, L. Wang, Efficient and high colour-purity green-light polymer light-emitting diodes (PLEDs) based on a PVK-supported Tb3+-containing metallopolymer, J. Mater. Chem. C. 5 (2017) 9021–9027. https://doi.org/10.1039/c7tc02092a.

[71]	H. Xin, F.Y. Li, M. Shi, Z.Q. Bian, C.H. Huang, Efficient electroluminescence from a new terbium complex, J. Am. Chem. Soc. 125 (2003) 7166–7167. https://doi.org/10.1021/ja034087a.

[72]	C. Pettinari, R. Pettinari, F. Marchetti, A. Drozdov, I. Timokhin, S. Semenov, S.I. Troyanov, The role of reaction medium on the coordination environment of terbium in complexes with 4-acylpyrazol-5-ones, Inorg. Chem. Commun. 6 (2003) 1423–1425. https://doi.org/10.1016/j.inoche.2003.08.028.

[73]	C. Pettinari, F. Marchetti, A. Cingolani, A. Drozdov, I. Timokhin, S.I. Troyanov, V. Tsaryuk, V. Zolin, Syntheses, structural and spectroscopic investigation (IR, NMR and luminescence) of new terbium and europium acylpyrazolonates, Inorganica Chim. Acta. 357 (2004) 4181–4190. https://doi.org/10.1016/j.ica.2004.06.024.

[74]	F. Marchetti, C. Pettinari, A. Pizzabiocca, A.A. Drozdov, S.I. Troyanov, C.O. Zhuravlev, S.N. Semenov, Y.A. Belousov, I.G. Timokhin, Syntheses, structures, and spectroscopy of mono- and polynuclear lanthanide complexes containing 4-acyl-pyrazolones and diphosphineoxide, Inorganica Chim. Acta. 363 (2010) 4038–4047. https://doi.org/10.1016/j.ica.2010.08.006.

[75]	I. V. Taydakov, Y.A. Belousov, K.A. Lyssenko, E. Varaksina, A.A. Drozdov, F. Marchetti, R. Pettinari, C. Pettinari, Synthesis, phosphorescence and luminescence properties of novel europium and gadolinium tris-acylpyrazolonate complexes, Inorganica Chim. Acta. 502 (2020) 119279. https://doi.org/10.1016/j.ica.2019.119279.

[76]	Y.A. Belousov, V.M. Korshunov, M.T. Metlin, D.A. Metlina, M.A. Kiskin, D.F. Aminev, N.P. Datskevich, A.A. Drozdov, C. Pettinari, F. Marchetti, I. V. Taydakov, Towards bright dysprosium emitters: Single and combined effects of environmental symmetry, deuteration, and gadolinium dilution, Dye. Pigment. 199 (2022) 110078. https://doi.org/10.1016/j.dyepig.2021.110078.

[77]	T. Polikovskiy, V. Korshunov, M. Metlin, V. Gontcharenko, D. Metlina, N. Datskevich, M. Kiskin, Y. Belousov, A. Tsorieva, I. Taydakov, Influence of Ligand Environment Stoichiometry on NIR-Luminescence Efficiency of Sm3+, Pr3+ and Nd3+ Ions Coordination Compounds, Molecules. 28 (2023) 5892. https://doi.org/10.3390/molecules28155892.

[78]	T. Polikovskiy, V. Korshunov, V. Gontcharenko, M. Kiskin, Y. Belousov, C. Pettinari, I. Taydakov, Dynamics of the Ligand Excited States Relaxation in Novel β-Diketonates of Non-Luminescent Trivalent Metal Ions, Int. J. Mol. Sci. 24 (2023) 1–22. https://doi.org/10.3390/ijms24098131.

[79]	C. Pettinari, F. Marchetti, R. Pettinari, A. Drozdov, S. Semenov, S.I. Troyanov, V. Zolin, No Title, Inorg. Chem. Commun. 9 (2006) 634–637. https://doi.org/10.1016/j.inoche.2006.03.008.

[80]	Y.A. Belousov, M.T. Metlin, D.A. Metlina, M.A. Kiskin, I.A. Yakushev, T.A. Polikovskiy, I. V. Taydakov, A.A. Drozdov, F. Marchetti, C. Pettinari, Self-Assembly of a Two-Dimensional Coordination Polymer Based on Silver and Lanthanide Tetrakis-Acylpyrazolonates: An Efficient New Strategy for Suppressing Ligand-to-Metal Charge Transfer Quenching of Europium Luminescence, Polymers (Basel). 15 (2023). https://doi.org/10.3390/polym15040867.

[81]	C. Pettinari, F. Marchetti, R. Pettinari, P. Natanti, A. Drozdov, S. Semenov, S.I. Troyanov, V. Zolin, Syntheses, spectroscopic characterization and X-ray structural studies of lanthanide complexes with adamantyl substituted 4-acylpyrazol-5-one, Inorganica Chim. Acta. 359 (2006) 4063–4070. https://doi.org/10.1016/j.ica.2006.04.045.

[82]	L.N. Bochkarev, A. V. Rozhkov, V.A. Ilichev, G.A. Abakumov, M.N. Bochkarev, Green-light emitting norbornene based terbium-containing copolymers. Synthesis, photo- and electroluminescent properties, Synth. Met. 190 (2014) 86–91. https://doi.org/10.1016/j.synthmet.2014.02.007.

[83]	L.I. Hui, H. Chun-hui, Z. Xin-sheng, X. Xiao-ming, X. Ling-ge, L.I. Tian-kai, Molecular Design and Langmuir-Blodgett Film Studies on a Series of New Nonlinear Optical Rare Earth Complexes, Langmuir. 10 (1994) 3794–3796. https://doi.org/10.1021/la00022a065.

[84]	Y. Huang, A. Yu, C.-H. Huang, L. Gan, X. Zhao, Y. Lin, B. Zhang, Microcavity Effect from a Novel Terbium Complex Langmuir-Blodgett Film, Adv. Mater. 11 (1999) 627–629. https://doi.org/10.1002/(SICI)1521-4095(199906)11:8<627::AID-ADMA627>3.0.CO;2-A.

[85]	H. Li, C.H. Huang, Y.F. Zhou, X.S. Zhao, O.H. Xia, T.K. Li, J. Bai, Synthesis, characterization, Langmuir-Blodgett film deposition and non-linear optical properties of a series of new non-linear optical materials based on azo dyes containing europium complex anions, J. Mater. Chem. 5 (1995) 1871–1878. https://doi.org/10.1039/JM9950501871.

[86]	H. Li, C. hui Huang, Y. lei Zhao, T. kai Li, J. Bai, X. sheng Zhao, X. hua Xia, Langmuir-Blodgett film and second harmonic generation of a series of new nonlinear optical rare earth complexes, Solid State Commun. 94 (1995) 731–733. https://doi.org/10.1016/0038-1098(95)00157-3.

[87]	Y.A. Belousov, V. V. Utochnikova, S.S. Kuznetsov, M.N. Andreev, V.D. Dolzhenko, A.A. Drozdov, New rare-earth metal acyl pyrazolonates: Synthesis, crystals structures, and luminescence properties, Russ. J. Coord. Chem. Khimiya. 40 (2014) 627–633. https://doi.org/10.1134/S1070328414090024.

[88]	C. Pettinari, F. Marchetti, R. Pettinari, Y.A. Belousov, I. V. Taydakov, V.D. Krasnobrov, D.I. Petukhov, A.A. Drozdov, Synthesis of novel lanthanide acylpyrazolonato ligands with long aliphatic chains and immobilization of the Tb complex on the surface of silica pre-modified via hydrophobic interactions, Dalt. Trans. 44 (2015) 14887–14895. https://doi.org/10.1039/c5dt01964h.

[89]	C. Pettinari, F. Marchetti, R. Pettinari, A. Drozdov, S. Troyanov, A.I. Voloshin, N.M. Shavaleev, Synthesis, structure and luminescence properties of new rare earth metal complexes with 1-phenyl-3-methyl-4-acylpyrazol-5-ones, J. Chem. Soc. Dalt. Trans. (2002) 1409–1415. https://doi.org/10.1039/b108058j.

[90]	A. Barkanov, A. Zakharova, T. Vlasova, E. Barkanova, A. Khomyakov, I. Avetissov, I. Taydakov, N. Datskevich, V. Goncharenko, R. Avetisov, NIR-OLED structures based on lanthanide coordination compounds: synthesis and luminescent properties, J. Mater. Sci. 57 (2022) 8393–8405. https://doi.org/10.1007/s10853-021-06721-4.

[91]	Z. Zhang, C. Yu, L. Liu, H. Li, Y. He, X. Lü, W.-K. Wong, R.A. Jones, Efficient near-infrared (NIR) luminescent PMMA-supported hybrid materials doped with tris-β-diketonate Ln3+ complex (Ln = Nd or Yb), J. Photochem. Photobiol. A Chem. 314 (2016) 104–113. https://doi.org/10.1016/j.jphotochem.2015.08.022.

[92]	Z. Zhang, L. Liu, C. Yu, H. Li, Y. He, X. Lü, W.K. Wong, R.A. Jones, PMMA-supported hybrid materials doped with highly near-infrared (NIR) luminescent neutral trikis-β-diketonate Yb3+ complex, Inorg. Chem. Commun. 52 (2015) 53–55. https://doi.org/10.1016/j.inoche.2014.12.018.

[93]	X. Zhang, L. Liu, C. Yu, H. Li, G. Fu, X. Lü, W.K. Wong, R.A. Jones, Highly efficient near-infrared (NIR) luminescent tris-β-diketonate Yb3 + complex in solution and in PMMA, Inorg. Chem. Commun. 70 (2016) 153–156. https://doi.org/10.1016/j.inoche.2016.06.006.

[94]	C. Yu, Z. Zhang, L. Liu, W. Feng, X. Lü, W.K. Wong, R.A. Jones, Near-infrared (NIR) luminescent PMMA-based hybrid materials doped with Ln-β-diketonate (Ln = Nd or Yb) complexes, Inorg. Chem. Commun. 49 (2014) 30–33. https://doi.org/10.1016/j.inoche.2014.09.008.

[95]	C. Yu, Z. Zhang, L. Liu, H. Li, Y. He, X. Lü, W.-K. Wong, R.A. Jones, PMMA-supported hybrid materials doped with highly near-infrared (NIR) luminescent complexes [Zn(L1)(Py)Ln(L2)3] (Ln = Nd, Yb or Er), New J. Chem. 39 (2015) 3698–3707. https://doi.org/10.1039/C4NJ02373K.

[96]	J. Guan, G. Fu, Y. He, X. Lü, Z. Song, Efficient near-infrared (NIR) luminescent [Zn(L1)(4-vinyl-Py)Yb(L2)3] complex monomer covalently-bonded into PMMA, Inorg. Chem. Commun. 91 (2018) 63–66. https://doi.org/10.1016/j.inoche.2018.03.002.

[97]	J. Jia‑Hui, L. Bin, M. Yin‑Shan, Z. Yi‑Quan, L. Hai‑Quan, L. Shan‑Shan, Crystal Structure, Magnetic Properties and Theoretical Investigation of a Dysprsoium Complex Based on 1⁃Phenyl⁃3⁃methyl⁃4⁃benzoyl⁃pyrazol⁃5⁃one, CHINESE J. Inorg. Chem. 37 (2021) 623–628. https://doi.org/10.11862/CJIC.2021.082.

[98]	C.H. Huang, K.Z. Wang, X.Y. Zhu, N.Z. Wu, G.X. Xu, Y. Xu, Y.Q. Liu, D.B. Zhu, Y.W. Liu, Z.Q. Xue, Optical and electrical properties of the Langmuir-Blodgett films prepared from a rare earth coordination compound, Solid State Commun. 90 (1994) 151–154. https://doi.org/10.1016/0038-1098(94)90332-8.

[99]	D.-J. Qian, H. Nakahara, K. Fukuda, K.-Z. Yang, Monolayer Assemblies and Optical Properties of Europium(III) Complexes with β-Diketones Containing Various Substituents, J. Colloid Interface Sci. 194 (1997) 174–182. https://doi.org/10.1006/jcis.1997.5080.

[100]	A.K. Nurtaeva, I.P. Efimov, Hydrate state of rare earth element phenylmethylbenzoylpyrazolonates, Russ. J. Inorg. Chem. 30 (1985) 1717–1721.

[101]	Z.-X. Long, H. Yang, X.-Y. Dai, S.-S. Liu, Crystal structure, Hirshfeld surface, luminescent properties and cytotoxicity of five mononuclear Ln-complexes based on 1⁃phenyl⁃3⁃methyl⁃4⁃benzoyl⁃5⁃pyrazolinone, J. Mol. Struct. 1307 (2024) 137943. https://doi.org/https://doi.org/10.1016/j.molstruc.2024.137943.

[102]	Z.-X. Long, W. Li, D.-F. Li, J.-H. Jing, S.-S. Liu, 发光性能与密度泛函理论计算, CHINESE J. Inorg. Chem. 39 (2023) 385–394. https://doi.org/10.11862/CJIC.2023.009.

[103]	E.I. Szerb, A. Crispini, M. La Deda, D. Pucci, P.F. Liguori, C. Pettinari, Europium(III) and terbium(III) luminescent lanthanidomesogens, Mol. Cryst. Liq. Cryst. 549 (2011) 86–99. https://doi.org/10.1080/15421406.2011.581149.

[104]	E.T. Karaseva, V.E. Karasev, A.A. Udovenko, N.I. Sigula, Crystal structure of an adduct of europium phenylmethylbenzoylpyrazolonate with triisobutyl phosphate. Relation of structural and luminescent-spectroscopic parameters in mixed europium chelates, Russ. J. Coord. Chem. Khimiya. 9 (1985) 692–698.

[105]	R. Van Deun, P. Nockemann, T.N. Parac-Vogt, K. Van Hecke, L. Van Meervelt, C. Görller-Walrand, K. Binnemans, Near-infrared photoluminescence of lanthanide complexes containing the hemicyanine chromophore, Polyhedron. 26 (2007) 5441–5447. https://doi.org/10.1016/j.poly.2007.08.005.

[106]	M.A. Pavier, T. Richardson, T.M. Searle, C.H. Huang, H. Li, D. Zhou, Photoluminescence study of Langmuir-Blodgett films of a hemicyanine molecular complex containing Yb3+, Supramol. Sci. 4 (1997) 437–441. https://doi.org/10.1016/S0968-5677(97)00043-6.

[107]	M.S. Weaver, D.G. Lidzey, M.A. Pavier, H. Mellor, S.L. Thorpe, D.D.C. Bradley, T. Richardson, T.M. Searle, C.H. Huang, H. Lui, D. Zhou, Organic light-emitting diodes (LEDs) based on Langmuir-Blodgett films containing rare-earth complexes, Synth. Met. 76 (1996) 91–93. https://doi.org/10.1016/0379-6779(95)03425-J.

[108]	M. Travadi, R.N. Jadeja, R.J. Butcher, M.S. Shekhawat, Neodymium based acylpyrazolone complexes: Synthesis and physicochemical characterizations, Inorganica Chim. Acta. 559 (2024) 121766. https://doi.org/10.1016/j.ica.2023.121766.

[109]	M. Atanassova, V. Kurteva, I. Billard, Coordination Chemistry of Europium(III) Ion Towards Acylpyrazolone Ligands, Anal. Sci. 31 (2015) 917–922. https://doi.org/10.2116/analsci.31.917.

[110]	X. Li, Z. Si, C. Pan, L. Zhou, Z. Li, X. Li, J. Tang, H. Zhang, Near-infrared luminescent properties and natural lifetime calculation of a novel Er3+ complex, Inorg. Chem. Commun. 12 (2009) 675–677. https://doi.org/10.1016/j.inoche.2009.05.022.

[111]	C. Pettinari, F. Marchetti, A. Cingolani, A. Drozdov, S. Troyanov, I. Timokhin, V. Vertlib, Lanthanide metal complexes containing the first structurally characterized β-diketonate acid stabilized by hydrogen bonding, Inorg. Chem. Commun. 6 (2003) 48–51. https://doi.org/10.1016/S1387-7003(02)00678-0.

[112]	Z. Yang, R. Tang, Z. Zhang, Synthesis and luminescent properties of Tb(III) complex with a novel pyrazolone ligand and its interaction with bovine serum albumin, J. Mol. Struct. 1030 (2012) 19–25. https://doi.org/10.1016/j.molstruc.2012.07.023.

[113]	W. Jiang, B. Lou, J. Wang, H. Lv, Z. Bian, C. Huang, The influence of triplet energy levels of bridging ligands on energy transfer processes in Ir(iii)/Eu(iii) dyads, Dalt. Trans. 40 (2011) 11410–11418. https://doi.org/10.1039/c1dt10968e.

[114]	Z. Zhao, M. Bian, C. Lin, X. Fu, G. Yu, H. Wei, Z. Liu, Z. Bian, C. Huang, Efficient green OLEDs achieved by a terbium(III) complex with photoluminescent quantum yield close to 100%, Sci. China Chem. 64 (2021) 1504–1509. https://doi.org/10.1007/s11426-021-1036-0.

[115]	A. Listkowski, W. Osińska, J. Mohanraj, M. Pietraszkiewicz, G. Dutkiewicz, T. Borowiak, Synthesis and photoluminescence properties of novel lanthanide complexes based on pyrazolone Schiff bases, Synth. Met. 162 (2012) 1285–1291. https://doi.org/10.1016/j.synthmet.2012.04.035.

[116]	E. Girotto, A. Pereira, C. Arantes, M. Cremona, A.J. Bortoluzzi, C.A.M. Salla, I.H. Bechtold, H. Gallardo, Efficient terbium complex based on a novel pyrazolone derivative ligand used in solution-processed OLEDs, J. Lumin. 208 (2019) 57–62. https://doi.org/10.1016/j.jlumin.2018.12.027.

[117]	G. Bombiere, A. Polo, W. Jia-Fu, W. Jinguang, X. Guang-Xian, Synthesis and characterization of a ytterbium complex with diphenylacetylpyrazolone Yb(DPAP)3·(H2O)2·3EtOH, Inorganica Chim. Acta. 132 (1987) 263–271. https://doi.org/10.1016/S0020-1693(00)81753-3.

[118]	R. Gou, Y. Wang, R. Yang, Y. Lan, Luminescent properties of terbium(III) and europium(III) complexes with six 4-acetyl-bispyrazolones, Chem. Res. Chinese Univ. 30 (2014) 190–193. https://doi.org/10.1007/s40242-014-3380-z.

[119]	X. Li, L. Yan, H. Wanyan, R. Yang, Chelate complexes of 1,3-bis-(1′-phenyl-3′-methyl-5′-pyrazolone-4′)-1,3-propanedione and 1,10-phenanthroline with lanthanide, Polyhedron. 12 (1993) 2021–2025. https://doi.org/10.1016/S0277-5387(00)81476-X.

[120]	X. Li, H. Wanyan, W. Dong, R. Yang, Synthesis of novel mixed-ligand complexes of lanthanide ions with 1,4-bis-(1′-phenyl-3′-methyl-5′-pyrazolone-4′)-1,4-butanedione and 1,10-phenanthroline and their UV, IR, 1H NMR, fluorescence and thermal analysis studies, Polyhedron. 9 (1990) 2285–2291. https://doi.org/10.1016/S0277-5387(00)86955-7.

[121]	S.N. Semenov, A. Yu, S. V Eliseeva, C. Pettinari, F. Marchetti, A. Drozdov, S.I. Troyanov, First direct assembly of molecular helical complexes into a coordination polymer w, (2008) 1992–1994. https://doi.org/10.1039/b719171e.

[122]	L. Yang, R. Yang, Synthesis and structure of didysprosium complexes with a tetraketone, J. Mol. Struct. 380 (1996) 75–84. https://doi.org/10.1016/0022-2860(95)09164-5.

[123]	X. Li, L. Yan, H. Wanyan, X. Li, R. Yang, Investigation on lanthanide binuclear complexes of 1,5-bis-(1′-phenyl-3′-methyl-5′-pyrazolone-4′)-1,5-pentanedione and 2,2′-bipyridine, Polyhedron. 13 (1994) 3317–3321. https://doi.org/10.1016/S0277-5387(00)83113-7.

[124]	X. Li, R. Yang, Synthesis of ion association complexes of lanthanide ions with 1,5-bis-(1′-phenyl-3′-methyl-5′-pyrazolone-4′)-1,5-pentanedione and cetyltrimethyl ammonium bromide and their UV, IR, 1H NMR, fluorescence and thermal analysis studies, Polyhedron. 11 (1992) 1545–1550. https://doi.org/10.1016/S0277-5387(00)83149-6.

[125]	L. Yang, R. Yang, Synthesis and structure of dinuclear complexes of terbium(III) with 4-acetalbispyrazolone, J. Coord. Chem. 33 (1994) 303–310. https://doi.org/10.1080/00958979408024290.

[126]	L. Yang, R. Yang, Synthesis and crystal structure of the dinuclear complex of 1,5-bis(1′-phenyl-3′-methyl-5′-pyrazolone-4′)-1,5-pentanedione with samarium, Polyhedron. 14 (1995) 507–510. https://doi.org/10.1016/0277-5387(94)00270-O.

[127]	J. Yang, H. Ge, N. Jie, X. Ren, N. Wang, H. Zou, Study on the co-luminescence system of Tb-Gd-BPMPHD-CTMAB and its analytical application, Spectrochim. Acta Part A Mol. Biomol. Spectrosc. 51 (1995) 185–195. https://doi.org/10.1016/0584-8539(94)E0102-G.

[128]	J. Yang, H. Ge, N. Jie, X. Ren, H. Zou, The luminescence system of yttrium(III)—BPMPHD—CTMAB and the determination of yttrium(III), Talanta. 41 (1994) 2055–2060. https://doi.org/10.1016/0039-9140(94)00178-2.

[129]	W. Kezhi, H. Chunhui, X. Guangxian, Z. Xinsheng, X. Xiaohua, W. Nianzu, X. Lingge, L. Tiankai, Optical properties of Langmuir-Blodgett film of hemicyanine containing the rare earth complex anion Dy(BPMPHD)-2, Thin Solid Films. 252 (1994) 139–144. https://doi.org/10.1016/0040-6090(94)90786-2.

[130]	J. Yang, H. Ge, N. Jie, X. Ren, C. Tong, J. Wang, Study of the fluorescence system thulium–bis(1′-phenyl-3′-methyl-5′-pyrazol-4′-one) hexanedione–cetyltrimethylammonium bromide and its analytical application, Analyst. 120 (1995) 1705–1708. https://doi.org/10.1039/AN9952001705.

[131]	J. Yang, H. Ge, N. Jie, X. Ren, N. Wang, H. Zou, Study on the co-luminescence system Sm-Gd-BPMPHD-CTMAB and its analytical application, Fresenius. J. Anal. Chem. 349 (1994) 728–733. https://doi.org/10.1007/BF00325647.

[132]	J. Yang, N. Jie, C. Lin, M. Wang, W. Ma, Determination of Lutetium by Fluorimetry, using BPMPHD and CTMAB, Mikrochim. Acta. 127 (1997) 85–88. https://doi.org/10.1007/bf01243169.

[133]	Y. Zhao, D. Zhou, G. Yao, C.-H. Huang, Strong Luminescent Terbium(III)−Pyrazolone Complexes and Their Langmuir−Blodgett Films, Langmuir. 13 (1997) 4060–4065. https://doi.org/10.1021/la970009n.

[134]	P.N. Remya, S. Biju, M.L.P. Reddy, A.H. Cowley, M. Findlater, 1D Molecular Ladder of the Ionic Complex of Terbium-4-Sebacoylbis(1-phenyl-3-methyl-5-pyrazolonate) and Sodium Dibenzo-18-Crown-6: Synthesis, Crystal Structure, and Photophysical Properties, Inorg. Chem. 47 (2008) 7396–7404. https://doi.org/10.1021/ic800615y.

[135]	T. Yoshikuni, Cerium complexes with phthaloylbis(pyrazolone) ligands as an efficient catalysts for cresols dioxygenation, J. Mol. Catal. A Chem. 148 (1999) 285–288. https://doi.org/10.1016/S1381-1169(99)00285-X.

[136]	J. Bao, C. Tang, R. Tang, Synthesis and luminescent properties of novel pyrazolone rare earth complexes, J. Rare Earths. 29 (2011) 15–19. https://doi.org/10.1016/S1002-0721(10)60398-5.

[137]	J. Xu, K.N. Raymond, Lord of the rings: An octameric lanthanum pyrazolonate cluster, Angew. Chemie - Int. Ed. 39 (2000) 2745–2747. https://doi.org/10.1002/1521-3773(20000804)39:15<2745::AID-ANIE2745>3.0.CO;2-Q.

[138]	V.B. Kurteva, B.L. Shivachev, R.P. Nikolova, S.D. Simova, L.M. Antonov, L.A. Lubenov, M.A. Petrova, Conformational behaviour of 3-methyl-4-(4-methylbenzoyl)-1-phenyl-pyrazol-5-one: A sudden story of three desmotropes, RSC Adv. 5 (2015) 73859–73867. https://doi.org/10.1039/c5ra11858a.

[139]	A.S. Amarasekara, O.S. Owereh, K.A. Lyssenko, T. V. Timofeeva, Structural tautomerism of 4-acylpyrazolone schiff bases and crystal structure of 5-methyl-2-phenyl-4-{1-[(pyridin-2-ylmethyl)-amino]-ethylidene}-2,4-dihydro-pyrazol-3-one, J. Struct. Chem. 50 (2009) 1159–1165. https://doi.org/10.1007/s10947-009-0170-4.

[140]	E.C. Okafor, A 1H and 13C-NMR spectral study of some 4-acyl-3-methyl-1-phenylpyrazol-5-ones in chloroform, Spectrochim. Acta Part A Mol. Spectrosc. 40 (1984) 397–401. https://doi.org/10.1016/0584-8539(84)80069-0.

[141]	E. Okafor, Observations on 1-phenyl-3-methyl-4-trifluoroacetylpyrazolone-5, a promising extracting agent, Talanta. 29 (1982) 275–278. https://doi.org/10.1016/0039-9140(82)80112-4.

[142]	S. Kunchandy, P. Indrasenan, Synthesis and IR spectral studies of some lanthanide nitrate complexes with 4-benzoyl-3-methyl-1-phenylpyrazol-5-one, Polyhedron. 9 (1990) 795–799. https://doi.org/10.1016/S0277-5387(00)81343-1.

[143]	D. Li, S. Xiong, T. Guo, D. Shu, H. Xiao, G. Li, D. Guo, Novel pyrazolone derivatives and corresponding europium(III) complexes: Synthesis and properties research, Dye. Pigment. 158 (2018) 28–35. https://doi.org/10.1016/j.dyepig.2018.05.020.

[144]	N.M. Sita, T.P. Rao, C.S.P. Iyer, A.D. Damodaran, Mixed-ligand complexes of lanthanide ions with 1-phenyl-3-methyl-4-benzoylpyrazolone-5 and some oxodonors, Synth. React. Inorg. Met. Chem. 28 (1998) 75–85. https://doi.org/10.1080/00945719809351655.

[145]	X. Xu, Z. Tang, Z. Guo, Y. Chen, N. Shi, Z. Ma, Y. Han, Study on the synthesis and crystal structure of tetrahyhrated tetraaquotris(4‐mono‐chloroacetylantipyrine)samarium (III) perchlorate, Chinese J. Chem. 13 (1995) 54–62. https://doi.org/10.1002/cjoc.19950130109.

[146]	Y. Akama, M. Kajitani, T. Sugiyama, A. Sugimori, Crystal Structure of Scandium Complex of 1-Phenyl-3-methyl-4-benzoyl-5-pyrazolone, Anal. Sci. 13 (1997) 155–157. https://doi.org/10.2116/analsci.13.155.

[147]	X.-L. Li, X. Niu, L.-F. He, X.-L. Feng, S.-M. Fang, L.-F. Han, L.-M. Zhou, H.-P. Xiao, Acylpyrazolonate-based lanthanide complexes: Synthesis, crystal structures and photoluminescence properties, Synth. Met. 161 (2011) 1063–1067. https://doi.org/10.1016/j.synthmet.2011.03.016.

[148]	C. Pettinari, F. Marchetti, R. Pettinari, A. Drozdov, S. Troyanov, A.I. Voloshin, N.M. Shavaleev, metal complexes with 1-phenyl-3-methyl-4-acylpyrazol-5-ones †, (2002) 1409–1415. https://doi.org/10.1039/b108058j.

[149]	W. Zhu, Q. Jiang, Z. Lu, X. Wei, M. Xie, D. Zou, T. Tsutsui, Red electroluminescence from a novel europium β-diketone complex with acylpyrazolone ligand, Synth. Met. 111 (2000) 445–447. https://doi.org/10.1016/S0379-6779(99)00396-3.

[150]	F. Marchetti, C. Pettinari, A. Pizzabiocca, A.A. Drozdov, S.I. Troyanov, C.O. Zhuravlev, S.N. Semenov, Y.A. Belousov, I.G. Timokhin, Syntheses, structures, and spectroscopy of mono- and polynuclear lanthanide complexes containing 4-acyl-pyrazolones and diphosphineoxide, Inorganica Chim. Acta. 363 (2010) 4038–4047. https://doi.org/10.1016/j.ica.2010.08.006.

[151]	C. Pettinari, F. Marchetti, R. Pettinari, A. Drozdov, S. Semenov, S.I. Troyanov, V. Zolin, A new rare-earth metal acylpyrazolonate containing the Zundel ion H 5 O þ 2 stabilized by strong hydrogen bonding, 9 (2006) 634–637. https://doi.org/10.1016/j.inoche.2006.03.008.

[152]	S. Cotton, Lanthanide and Actinide Chemistry, John Wiley & Sons, Ltd, Chichester, UK, 2006. https://doi.org/10.1002/0470010088.

[153]	C.K. Jorgensen, R. Reisfeldt, JUDD-OFELT PARAMETERS AND CHEMICAL BONDING*, 1983.

[154]	E.T. Karaseva, A.P. Golovina, M.I. Gromova, I.P. Efimov, Luminescence of rare earth element chelates with phenylmethylpyrazolone derivatives, Russ. J. Coord. Chem. Khimiya. 1 (1975) 260–265.

[155]	D. Kovacs, K.E. Borbas, The role of photoinduced electron transfer in the quenching of sensitized Europium emission, Coord. Chem. Rev. 364 (2018) 1–9. https://doi.org/10.1016/j.ccr.2018.03.004.

[156]	M. Latva, H. Takalob, V.M. Mukkala, C. Matachescu, J.C. Rodríguez-Ubis, J. Kankare, Correlation between the lowest triplet state energy level of the ligand and lanthanide(III) luminescence quantum yield, J. Lumin. 75 (1997) 149–169. https://doi.org/10.1016/S0022-2313(97)00113-0.

[157]	S. Tobita, M. Arakawa, I. Tanaka, The paramagnetic metal effect on the ligand localized S1 .apprx. .fwdarw. T1 intersystem crossing in the rare-earth-metal complexes with methyl salicylate, J. Phys. Chem. 89 (1985) 5649–5654. https://doi.org/10.1021/j100272a015.

[158]	I. V. Taydakov, V.M. Korshunov, Y.A. Belousov, Y. V. Nelyubina, F. Marchetti, R. Pettinari, C. Pettinari, Synthesis, crystal structure and photophysical properties of mixed-ligand lanthanide complexes with 1,3-diketonates bearing pyrazole moieties and 1,10-phenanthroline, Inorganica Chim. Acta. 513 (2020) 119922. https://doi.org/10.1016/j.ica.2020.119922.

[159]	M.T. Metlin, D.O. Goryachii, D.F. Aminev, N.P. Datskevich, V.M. Korshunov, D.A. Metlina, A.A. Pavlov, L. V Mikhalchenko, M.A. Kiskin, V. V Garaeva, I. V Taydakov, Dyes and Pigments Bright Yb 3 + complexes for efficient pure near-infrared OLEDs, Dye. Pigment. 195 (2021) 109701. https://doi.org/10.1016/j.dyepig.2021.109701.

[160]	C. Hansch, A. Leo, R.W. Taft, A Survey of Hammett Substituent Constants and Resonance and Field Parameters, Chem. Rev. 91 (1991) 165–195. https://doi.org/10.1021/cr00002a004.

[161]	V.I. Tsaryuk, K.P. Zhuravlev, P. Gawryszewska, Processes of luminescence quenching in europium aromatic carboxylates with the participation of LMCT states: A brief review, Coord. Chem. Rev. 489 (2023) 215206. https://doi.org/10.1016/j.ccr.2023.215206.

[162]	Y.A. Belousov, V. V. Utochnikova, S.S. Kuznetsov, M.N. Andreev, V.D. Dolzhenko, A.A. Drozdov, New rare-earth metal acyl pyrazolonates: Synthesis, crystals structures, and luminescence properties, Russ. J. Coord. Chem. Khimiya. 40 (2014) 627–633. https://doi.org/10.1134/S1070328414090024.

[163]	M. Atanassova, R. Kukeva, Improvement of Gd(III) Solvent Extraction by 4-Benzoyl-3-methyl-1-phenyl-2-pyrazolin-5-one: Non-Aqueous Systems, Separations. 10 (2023). https://doi.org/10.3390/separations10050286.

[164]	A. Roy, K. Nag, Solvent extraction behavior of rare earth ions with 1-phenyl-3-methyl-4-benzoyl-5-pyrazolone—II, J. Inorg. Nucl. Chem. 40 (1978) 331–334. https://doi.org/10.1016/0022-1902(78)80133-X.

[165]	K. Nag, SOLVENT EXTRACTION, Solvent Extr. Ion Exch. 1 (1983) 413–451. https://doi.org/10.1080/07366298308918407.

[166]	L. Jian-Min, Y. Ru-Dong, M. Yong-Xiang, Extractive Separation of Scandium , Yttrium , Lanthanum , Iron , and Tin in Hydrochloric Acid System with 1 , 10-, Chem. Pap. 3 (1992) 290–292.

[167]	M.M. Saeed, M.A. Qayyum, A. Ali, Synergic extraction of Eu(III) with 3-methyl-1-phenyl-4-trifluoroacetyl-2-pyrazolin-5-one (HPMTFP) and tribenzylamine (TBA) from perchlorate media, Radiochim. Acta. 76 (1997) 205–209. https://doi.org/10.1524/ract.1997.76.4.205.

[168]	G. Ma, H. Freiser, S. Muralidharan, Interfacial Catalysis of Formation and Dissociation of Tervalent Lanthanide Complexes in Two-Phase Systems, Anal. Chem. 69 (1997) 2827–2834. https://doi.org/10.1021/ac961191k.

[169]	Y.C. Xing, W.J. Dong, X.L. Li, R.D. Yang, Study of the complexing of lanthanide ions with 1-phenyl-3-methyl-4-heptaflurobutyryl pyrazolone-5 and triphenylphosphine oxide by the two-phase titration method, J. Coord. Chem. 22 (1990) 71–78. https://doi.org/10.1080/00958979009408209.

[170]	R.L. Varma, S. Sujatha, M.L.P. Reddy, T.P. Rao, C.S.P. Lyer, A.D. Damodaran, Bis(2-ethylhexyl)-N,N-diethylcarbamoylmethyl phosphonate as a Synergist in the Extraction of Trivalent Lanthanides by 1-Phenyl-3-methyl-4-trifluoroacetyl-py razolone-5, Ract. 72 (1996) 133–136. https://doi.org/10.1524/ract.1996.72.3.133.

[171]	Z. Kolařík, Acidic organophosphorus extractants — XIII, J. Inorg. Nucl. Chem. 33 (1971) 1135–1138. https://doi.org/10.1016/0022-1902(71)80182-3.

[172]	S. Umetani, Y. Kawase, Q.T.H. Le, M. Matsui, The Synergistic Extraction of Lanthanides with Trifluoroacetylcycloalkanones and Trioctylphosphine Oxide, Chem. Lett. 26 (1997) 771–772. https://doi.org/10.1246/cl.1997.771.

[173]	P.B. Santhi, M.L. P-Reddy, T.R. Ramamohan, A.D. Damodaran, J.N. Mathur, M.S. Murali, R.H. Iyer, Synergistic solvent extraction of trivalent lanthanides and actinide by mixtures of 1-phenyl-3-methyl-4-benzoyl-pyra2alone-5 and neutral oxo-donors, Solvent Extr. Ion Exch. 12 (1994) 633–650. https://doi.org/10.1080/07366299408918229.

[174]	A.N. Turanov, V.K. Karandashev, D. V. Baulin, V.E. Baulin, A.Y. Tsivadze, Extraction of Rare Earth Elements(III) with Mixtures of 1-Phenyl-3-methyl-4-benzoyl-5-pyrazolone and 2-Phosphorylphenoxyacetamides, Russ. J. Inorg. Chem. 64 (2019) 407–413. https://doi.org/10.1134/S0036023619030203.

[175]	R.H. Wharf, G.R. Choppin, D.J. Pruett, SYNERGISTIC SOLVENT EXTRACTION OF AM(III) AND EU(III) WITH THE SOFT DONOR TRIISOBUTYLPHOSPHINE SULFIDE AND THENOYLTRIFLUOROACETONE, Solvent Extr. Ion Exch. 8 (1990) 615–627. https://doi.org/10.1080/07366299008918020.

[176]	J. Gao, Thermodynamic investigations of aqueous-molten paraffin wax liquid—liquid extractions and synergistic extractions of some trivalent rare earth elements, Talanta. 41 (1994) 541–546. https://doi.org/10.1016/0039-9140(93)E0021-5.

[177]	A.N. Turanov, A.G. Matveeva, I. Yu, M.P. Pasechnik, S. V Matveev, M.I. Godovikova, T. V Baulina, V.K. Karandashev, V.K. Brel, Tripodal organophosphorus ligands as synergistic agents in the solvent extraction of lanthanides ( III ). Structure of mixed complexes and effect of diluents, Polyhedron. 161 (2019) 276–288. https://doi.org/10.1016/j.poly.2019.01.036.

[178]	M.A. Pavier, M.S. Weaver, D. Lidzey, T. Richardson, T.M. Searle, D.D.C. Bradley, C.H. Huang, H. Li, D. Zhou, Electroluminescence from dysprosium- and neodymium-containing LB films, Thin Solid Films. 284–285 (1996) 644–647. https://doi.org/10.1016/S0040-6090(95)08411-8.

[179]	D.G. Moon, O. V. Salata, M. Etchells, P.J. Dobson, V. Christou, Efficient single layer organic light emitting diodes based on a terbium pyrazolone complex, Synth. Met. 123 (2001) 355–357. https://doi.org/10.1016/S0379-6779(01)00306-X.

[180]	G. Yu, F. Ding, H. Wei, Z. Zhao, Z. Liu, Z. Bian, L. Xiao, C. Huang, Highly efficient terbium(III)-based organic light-emitting diodes obtained by exciton confinement, J. Mater. Chem. C. 4 (2015) 121–125. https://doi.org/10.1039/c5tc02944a.

[181]	D.Q. Gao, Y.Y. Huang, C.H. Huang, F.Y. Li, L. Huang, Green exciplex emission from a bilayer light-emitting diode containing a rare earth ternary complex, Chem. Phys. Lett. 350 (2001) 206–210. https://doi.org/10.1016/S0009-2614(01)01269-6.

[182]	O. Renault, O. V. Salata, M. Etchells, P.J. Dobson, V. Christou, Low reflectivity multilayer cathode for organic light-emitting diodes, Thin Solid Films. 379 (2000) 195–198. https://doi.org/10.1016/S0040-6090(00)01558-3.