Supporting Information

Magnetism of TbPc2 on ferromagnetic iron oxide surface.

Niccolò Giaconi,1 Leonardo Tacconi,1 Fabio Santanni,1 Marta Albanesi,1 Guglielmo Pio Cesare Battista Albani,2 Isheta Majumdar,2 Luca Schio,3 Matteo Briganti,1 Gianlorenzo Bussetti,2 Edwige Otero,4 Luca Floreano,3 Andrea Caneschi,1,5 Matteo Mannini,1 Giulia Serrano,1,5 Alberto Calloni,2* Lorenzo Poggini.1,6*

1 Department of Chemistry “Ugo Schiff” DICUS & INSTM Research Unit, University of Florence, Via della Lastruccia 3-13, 50019, Sesto Fiorentino, Italy.

2 Department of Physics, Politecnico di Milano, Piazza Leonardo da Vinci 32, Milan, 20133, Italy.

3 Istituto Officina dei Materiali – CNR-IOM Laboratorio TASC s.s. 14 km 163.5, 34149 Trieste, Italy4 Synchrotron-SOLEIL, L'Orme des Merisiers, Saint-Aubin, 91192 France.

5 Department of Industrial Engineering – DIEF – and INSTM Research Unit, University of Florence, Via Santa Marta 3, Florence, 50139 Italy.

6 Institute for Chemistry of Organo-Metallic Compounds (ICCOM-CNR), Via Madonna del Piano, Sesto Fiorentino, Firenze, 50019 Italy

Figure S1. STM image of the ultra-thin FeO layer grown on Fe(001) (dimension 250x150nm2, It=150pA, Vb= 500mV).

Figure S2. a) Simulated and experimental XNLD spectrum at the Tb M4,5 edge; b) XMCD spectra at the Tb M4,5 edge collected at 0° and 45° degree; c) and d) Simulated vs Experimental intensity of XMCD at the Tb M4,5 edge at 0° and 45° degree, respectively

Figure S3. a) XMCD spectra at the Fe L2,3 edge at theta 0° and b) at theta 45°. c) Hysteresis loop recorded at the Fe L2,3 edge at angle (q) 0° and at 45°.

Table S1. Comparison between the simulated and the experimental XMCD percentages at the Tb M5 edge, collected at 0° and 45°, and the relative intensity variation.

|  | 0° (%) | 45° (%) | Variation |
| --- | --- | --- | --- |
| XMCD experimental | -156.6 | -136.8 | +19.3 (10%) |
| XMCD simulated | -184 | -160.7 | +19.8 (12.6%) |

Figure S4. a) XMCD (σ- - σ + ) (blue line) spectrum acquired at the Fe L2,3 edge and the resulting integration (red line); b)(σ++σ - )/2 spectra (blue curve) with a double step baseline and the resulting integrated curve (red line).

The moments and the morb/mspin ratio were calculated as reported in ref [1]:

morb=-4q*n3d6r

mspin=-(6p-4q)*n3d2r

where n3d is the number of d holes, p and q are the integrated areas of the XMCD spectrum at the L3 and L2 edges, respectively, while r corresponds to the total area of the (σ-+σ+)/2  spectrum after subtraction of a double step baseline (with a step height ratio L3:L2 of 2:1). From this analysis, by imposing n3d = 3.39  we estimated morb = 0.08 µB,  mspin = 2.217 µB and the resulting ratio morb/mspin = 0.034.

Table S2. Parameters employed during simulations of polarised XAS spectra. Parameters with the subscript i refer to the initial electronic state 3d104f8, while those with the subscript f refer to the final electronic state 3d94f9. The letters d and f in parentheses indicate the electronic shell on which the parameters act.

| Parameter | Value (eV) | Parameter | Value (eV) |
| --- | --- | --- | --- |
| Fi2f | 11.929 | Ff6f | 5.640 |
| Fi4f | 7.486 | Ff2df | 8.042 |
| Fi6f | 5.386 | Ff4df | 3.766 |
| ζif | 0.221 | Gf1df | 5.788 |
| B20 | 0.0515 | Gf3df | 3.394 |
| B40 | -0.0283 | Gf5df | 2.345 |
| B60 | 0.00382 | ζff | 0.251 |
| Ff2f | 12.468 | ζfd | 13.368 |
| Ff4f | 7.834 |  |  |

Table S3. Comprehensive table summarizing literature data on the deposition of TbPc₂ SMM on different substrates and their physicochemical properties.

| Substrate | Electronic Nature | Band Gap (Eg​) | Thickness | Observed TbPc₂ Magnetic Behaviour | Interaction Mechanism | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| FeO / Fe(001) | Correlated Metallic Overlayer (Substrate-hybridized 3d bands) | ~0 eV | 1 ML | Preserved Magnetic Behaviour/ Quenched Hysteresis | f-π-d hybridization; mediated exchange via narrowed 3d-states. | [2- this paper] |
| MgO / Ag(100) | Wide-gap Insulator | ~7.8 eV | 1–5 ML | Preserved SMM / Giant Butterfly Hysteresis | Pure electronic decoupling; suppression of substrate-mediated relaxation. | [3] |
| TiO₂ / Ag(100) | Band Insulator | ~3.0 eV | 1 ML (Lepidocrocite) | Preserved SMM / Small Butterfly Hysteresis | Partial decoupling; efficiency comparable to Graphene. | [4] |
| Graphene / SiC(0001) | Semi-metal (Dirac Cone, Zero gap) | 0 eV | 1 ML | Preserved SMM / Small Butterfly Hysteresis | Weak π-π interaction; weak coupling to the metallic substrate. | [5] |
| Au(111) | Metal (Noble, highly delocalized s/p bands) | 0 eV | Bulk | Quenched Hysteresis / Kondo Effect | Strong hybridisation; direct exchange screening by conduction electrons. | [6] |

References

[1]	 Chen C T,  et al.,  Phys. Rev. Lett. 75 152–5. DOI:10.1103/PhysRevLett.75.152

[2] This paper;

[3] C. Wäckerlin et al., Adv. Mater., 2016, 28, 5195–5199. DOI: 10.1002/adma.201506305

[4] A.L Sorrentino et al., J. Mat. Chem. C, 2021, 9, 14949–14958. DOI: 10.1039/D1TC03408A

[5] G. serrano et al., Nanoscale, 2018, 10, 2733–2740. DOI: 10.1039/C7NR08372F

[6] K. Katoh et al., ", JACS, 2009, 131, 9967–9976. DOI: 10.1021/ja902349t